## Slide 1: Chapter 18: Electrical Properties
ISSUES TO ADDRESS...
• How are electrical conductance and resistance
characterized?
• What are the physical phenomena that distinguish
conductors, semiconductors, and insulators?
• For metals, how is conductivity affected by
imperfections, T, and deformation?
• For semiconductors, how is conductivity affected
by impurities (doping) and T?

## Slide 2: View of an Integrated Circuit
• Scanning electron microscope images of an IC:
• EDS map showing location of Si (a semiconductor):
-- Si shows up as light regions.
• EDS map showing location of Al (a conductor):
-- Al shows up as light regions.
(b)
(c)
0.5 mm
(a)
(d)
45 mm
Al
Si
(doped)
(d)

## Slide 3: Electrical Conduction
• Ohm's Law:
V = I R
voltage drop (volts = J/C)
C = Coulomb
resistance (Ohms)
current (amps = C/s)
• Conductivity, σ
• Resistivity, ρ: -- a material property that is independent of sample size and geometry
cross-sectional area
of current flow
current flow path length

## Slide 4: Electrical Conduction
• Resistance:
• Ohm's Law:
DV = I R
voltage drop (volts)
C = Coulomb
resistance (Ohms)
current (amps = C/s)
I
e
-
A
(cross
sect.
area)
DV
L
Resitivity: r (Ohm-m)
Conductivity: 1/r (Ohm-m)-1

## Slide 5: Electrical Properties
Which will have the greater resistance?
Analogous to flow of water in a pipe
Resistance depends on sample geometry and size.
D
2D
2

## Slide 6: Definitions
Further definitions
  J =   <= another way to state Ohm’s law
  J  current density = current / area = I/A
    electric field = V/L or (V/ L )
Current carriers
  electrons in most solids
  ions can also carry (particularly in liquid solutions)
Electron flux conductivity voltage gradient
J =  (V/L)

## Slide 7: Conductivity: Comparison
• Room T values (Ohm-m)
-1
Silver
6.8 x 10
7
Copper
6.0 x 10
7
Iron
1.0 x 10
7
METALS
conductors
Silicon
4 x 10
-4
Germanium
2 x 10
0
GaAs
10
-6
SEMICONDUCTORS
    = ( - m)
-1
Polystyrene <10
-14
Polyethylene 10
-15
-10
-17
Soda-lime glass 10
Concrete 10
-9
Aluminum oxide <10
-13
CERAMICS
POLYMERS
insulators
-10
-10
-11
= S/m
PEDOT
10
4
semiconductors

## Slide 8: Example: Conductivity Problem
What is the minimum diameter (D) of the wire so that DV < 1.5 V?
100m
Cu wire
I = 2.5A
-
+
e
-
DV
Solve to get D > 1.87 mm
< 1.5V
2.5A
6.07 x 10 (Ohm-m)
7
-1
100m

## Slide 9: Electronic Band Structures
Notes:   So the individual atomic energy levels interact to form molecular energy levels

## Slide 10: Band Structure
Valence band – filled – highest occupied energy levels: HOMO
Conduction band – empty – lowest unoccupied energy levels: LUMO
valence band
Conduction band
Notes: contains valence electrons from the atoms

## Slide 11: Energy levels of electrons
Highest energy level: Ef = Fermi energy
If Ef is located within a band, then metal
If Ef at the top of a band, with a small band gap (Eg < 2 eV), then semiconductor
If Ef at the top of a band, with a large band gap (Eg > 2 eV), then insulator

## Slide 12: Conduction & Electron Transport
• Metals (Conductors):
-- Thermal energy puts
many electrons into
a higher energy state.
• Energy States:
-- for metals nearby
energy states
are accessible
by thermal
fluctuations.
+
-
-
filled
band
Energy
partly
filled
valence
band
empty
band
GAP
filled states
Energy
filled
band
filled
valence
band
empty
band
filled states

## Slide 13: Energy States: Insulators & Semiconductors
• Insulators:
-- Higher energy states not
accessible due to gap (> 2 eV).
Energy
filled
band
filled
valence
band
empty
band
filled states
GAP
• Semiconductors:
-- Higher energy states separated
by smaller gap (< 2 eV).
Energy
filled
band
filled
valence
band
empty
band
filled states
GAP
?

## Slide 14: Charge Carriers
Two charge carrying mechanisms
  Electron – negative charge
  Hole – equal & opposite positive charge
Move at different speeds - drift velocity
Higher temp. promotes more electrons into the conduction band
  as T
Electrons scattered by impurities, grain boundaries, etc.

## Slide 15: Band structure and color
Metals: no band gap, don’t allow for visible light (photons) to propagate: appear shiny, silvery. Some (Au, Cu) do show certain colors due to absorptions
Semiconductors: Absorb photons with energies similar to those of band gaps; may be dark or colored. Visible photons go from ~1.8 eV (red) to ~3.1 eV (violet).
Insulators: have large band gaps, are often clear or white (scattering)

## Slide 16: Metals: Resistivity vs T, Impurities
• Imperfections increase resistivity
-- grain boundaries
-- dislocations
-- impurity atoms
-- vacancies
These act to scatter
electrons so that they
take a less direct path.
• Resistivity
increases with:
-- temperature
-- wt% impurity
-- %CW
 = thermal + impurity + deformation
deformed Cu + 1.12 at%Ni
T (°C)
-200
-100
0
Cu + 3.32 at%Ni
Cu + 2.16 at%Ni
1
2
3
4
5
6
Resistivity,
r
(10
-8
Ohm-m)
0
Cu + 1.12 at%Ni
“Pure” Cu

## Slide 17: Estimating Conductivity
Adapted from Fig. 7.16(b), Callister 7e.
• Question:
-- Estimate the electrical conductivity  of a Cu-Ni alloy
that has a yield strength of 125 MPa.
Yield strength (MPa)
wt. %Ni, (Concentration C)
0
10
20
30
40
50
60
80
100
120
140
160
180
21 wt%Ni
wt. %Ni, (Concentration C)
Resistivity,
r
(10
-8
Ohm-m)
10
20
30
40
50
0
10
20
30
40
50
0
125
CNi = 21 wt%Ni
From step 1:
30

## Slide 18: Intrinsic Semiconductors: Conductivity vs T
• Data for Pure Silicon:
-- σ increases with T
-- opposite to metals
Adapted from Fig. 18.16, Callister & Rethwisch 9e.
material
Si
Ge
GaP
CdS
band gap (eV)
1.11
0.67
2.25
2.40

## Slide 19: Pure Semiconductors: Conductivity vs T
• Data for Pure Silicon:
-- s increases with T
-- opposite to metals
electrical conductivity,
s
(Ohm-m)
-1
50
10
0
1
000
10
-2
10
-1
10
0
10
1
10
2
10
3
10
4
pure
(undoped)
T(K)
electrons
can cross
gap at
higher T
material
Si
Ge
GaP
CdS
band gap (eV)
1.11
0.67
2.25
2.40
Energy
filled
band
filled
valence
band
empty
band
filled states
GAP
?

## Slide 20: Conduction in Terms of Electron and Hole Migration
electric field
electric field
electric field
• Electrical Conductivity given by:
# electrons/m
3
electron mobility
# holes/m
3
hole mobility
• Concept of electrons and holes:
+
-
electron
hole
pair creation
+
-
no applied
applied
valence
electron
Si atom
applied
electron
hole
pair migration

## Slide 21: Intrinsic vs Extrinsic Conduction
• Intrinsic:
# electrons = # holes (n = p)
--case for pure Si, Ge
• Extrinsic:
--n ≠ p
--occurs when impurities are added with a different
# valence electrons than the host (e.g., Si atoms)
• n-type Extrinsic: (n >> p)
no applied
electric field
5+
4
+
4
+
4
+
4
+
4
+
4
+
4
+
4
+
4
+
4
+
4
+
Phosphorus atom
valence
electron
Si atom
conduction
electron
hole
• p-type Extrinsic: (p >> n)
no applied
electric field
Boron atom
3
+
4
+
4
+
4
+
4
+
4
+
4
+
4
+
4
+
4
+
4
+
4
+

## Slide 22: Extrinsic Semiconductors: Conductivity vs. Temperature
• Data for Doped Silicon:
-- σ increases doping
-- reason: imperfection sites
lower the activation energy to
produce mobile electrons.
• Comparison: intrinsic vs
extrinsic conduction...
-- extrinsic doping level:
1021/m3 of a n-type donor
impurity (such as P).
-- for T < 100 K: "freeze-out“,
thermal energy insufficient to
excite electrons.
-- for 150 K < T < 450 K: "extrinsic"
-- for T >> 450 K: "intrinsic"
Conduction electron
concentration (1021/m3)
T
(K)
600
400
200
0
0
1
2
3
freeze-out
extrinsic
intrinsic
doped
undoped

## Slide 23: p-n Rectifying Junction: Diode
• Allows flow of electrons in one direction only (e.g., useful
to convert alternating current to direct current.
• Processing: diffuse P into one side of a B-doped crystal.
• Results:
--No applied potential:
no net current flow.
--Forward bias: carrier
flow through p-type and
n-type regions; holes and
electrons recombine at
p-n junction; current flows.
--Reverse bias: carrier
flow away from p-n junction;
carrier conc. greatly reduced
at junction; little current flow.
+
+
+
+
+
-
-
-
-
-
p-type
n-type
+
-
+
+
+
+
+
-
-
-
-
-
p-type
n-type
+
+
+
+
+
-
-
-
-
-
p-type
n-type
-
+

## Slide 24: Properties of Rectifying Junction

## Slide 25: Intrinsic Semiconductors
Pure material semiconductors: e.g., silicon & germanium
  Group IVA materials
Compound semiconductors
  III-V compounds
    Ex: GaAs & InSb
  II-VI compounds
    Ex: CdS & ZnTe
  The wider the electronegativity difference between the elements the wider the energy gap.

## Slide 26: Doped Semiconductor: Conductivity vs. T
• Data for Doped Silicon:
-- s increases doping
-- reason: imperfection sites
lower the activation energy to
produce mobile electrons.
doped
0.0013at%B
0.0052at%B
electrical conductivity,
s
(Ohm-m)
-1
50
10
0
1
000
10
-2
10
-1
10
0
10
1
10
2
10
3
10
4
pure
(undoped)
T(K)
• Comparison: intrinsic vs
extrinsic conduction...
-- extrinsic doping level:
1021/m3 of a n-type donor
impurity (such as P).
-- for T < 100 K: "freeze-out“,
thermal energy insufficient to
excite electrons.
-- for 150 K < T < 450 K: "extrinsic"
-- for T >> 450 K: "intrinsic"
conduction electron
concentration (1021/m3)
T
(K)
600
400
200
0
0
1
2
3
freeze-out
extrinsic
intrinsic
doped
undoped

## Slide 27: Number of Charge Carriers
Intrinsic Conductivity
   = n|e|e + p|e|h
For GaAs n = 4.8 x 1024 m-3
For Si n = 1.3 x 1016 m-3
for intrinsic semiconductor n = p
  = n|e|(e + h)
Ex: GaAs

## Slide 28: Junction Transistor
Fig. 18.24, Callister 7e.

## Slide 29: MOSFET Transistor Integrated Circuit Device
Integrated circuits - state of the art ca. 50 nm line width
  ~ 1,000,000,000 components on chip
  chips formed one layer at a time
Fig. 18.26, Callister & Rethwisch 9e.
MOSFET (metal oxide semiconductor field effect transistor)

## Slide 30: Integrated Circuit Devices: FET

## Slide 31: Solid-State Semiconductor Devices

## Slide 32: Solid-State Semiconductor Devices

## Slide 33: Solid-State Semiconductor Devices

## Slide 34: Silicon single crystals

## Slide 35: Czochralski process
Currently 300 mm (12 inch) wide x 775 mm thick
450 mm (18 inch) x 925 mm in development

## Slide 36: Wafers: single crystal Si slices
2-inch (51 mm), 4-inch (100 mm), 6-inch (150 mm), and 8-inch (200 mm) wafers
Larger wafers (200 mm and up)
only have a single notch
a=0.5431 nm

## Slide 37: Photolithography

## Slide 38: Doping

## Slide 39: Ionic Conduction
Charged anions and cations can respond to electric fields and
contribute to current if they are sufficiently mobile
+
=
Important in certain ceramics, electrolytes, conjugated polymers

## Slide 40: Ferroelectric Ceramics
Ferroelectric Ceramics are dipolar below Curie TC = 120ºC
cooled below Tc in strong electric field - make material with strong dipole moment

## Slide 41: Piezoelectric Materials
at rest
compression induces voltage
applied voltage induces expansion
Piezoelectricity – application of pressure produces current

## Slide 42: Capacitance

## Slide 43: Dielectric properties

## Slide 44: Photovoltaics
Light Emitting Diodes: (LEDs)
Reverse this process: current in, light out
light in
current out

## Slide 45: Tuning Band Gaps with Alloys
Lattice constant (Angstroms)

## Slide 46: Tuning Band Gaps with Alloys

## Slide 47: Tune crystal with composition
Atomic fraction

## Slide 48: Thermoelectrics

## Slide 49: Thermoelectric Applications
Electricity in
Heat out
Heat in
Electricity out

## Slide 50: Summary
• Electrical conductivity and resistivity are:
-- material parameters.
-- geometry independent.
• Electrical resistance is:
-- a geometry and material dependent parameter.
• Conductors, semiconductors, and insulators...
-- differ in accessibility of energy states for
conductance electrons.
• For metals, conductivity is increased by
-- reducing deformation
-- reducing imperfections
-- decreasing temperature.
• For pure semiconductors, conductivity is increased by
-- increasing temperature
-- doping (e.g., adding B to Si (p-type) or P to Si (n-type).

## Slide 51: HW #12: Last One
In the Chat section of the course web site on
Canvas, post a question about any aspect of
the course. On the last day of class next Tuesday,
the instructor will do his best to answer as many of
these questions as possible. We will give a full homework assignment credit to all students who post a question.

## Slide 52
Example Grading scale from 2010
A+ 830
A 791
A- 757
B+ 701
B 636
B- 603
C+ 564
C 534
C- 511
D+ 468
D 409
E <400
A+
A
A-
B+
B
B-
B-
E
D
D+
C-
C
C
C+
HW: 150
M1: 250
M2: 250
Final: 350
Tot: 1000
Specific numbers will be different this year
but overall distribution likely similar