## Slide 1
Exams will be
returned in class
Thursday

## Slide 2: Tips
Come to office hours
Ask questions in class or on chat room
Do HW, try unassigned homework problems in text or on WileyPlus
Read other textbooks, web sites
Time management: maximize points
Units are important
Focus on the subject matter, not the exams
Final Exam is 35%, Thursday May 17th, 1-3 PM

## Slide 3: Chapter 16: Composite Materials
ISSUES TO ADDRESS...
• What are the classes and types of composites?
• Why are composites used instead of just metals,
ceramics, or polymers?
• How do we estimate composite stiffness & strength?
• What are some typical processes and applications?

## Slide 4: Composites
Combine different materials with the objective of getting a more desirable combination of properties
  Ex: get flexibility & light weight of a polymer plus the strength of a ceramic
Principle of combined action
  Mixture gives “averaged” properties
Steels, other alloys are really “composites”, but term is usually used to describe materials where the separate components are mixed together later
Notes:   Don’t always get what you want
    Ex: combine ferret (pet) + mink (fur)
      Desire a mink with good disposition but got a nasty ferret

## Slide 5: Terminology/Classification
• Composites:
-- Multiphase material w/significant
proportions of each phase.
• Dispersed phase:
-- Purpose: enhance matrix properties.
MMC: increase sy, TS, creep resist.
CMC: increase Kc
PMC: increase E, sy, TS, creep resist.
-- Classification: Particle, fiber, structural
• Matrix:
-- The continuous phase
-- Purpose is to:
- transfer stress to other phases
- protect phases from environment
-- Classification: MMC, CMC, PMC
metal
ceramic
polymer
woven
fibers
cross
section
view
0.5
mm
0.5
mm

## Slide 6: Composite Survey

## Slide 7: Composite Survey: Particle-I
• Examples:
- Spheroidite
steel
matrix:
ferrite (a)
(ductile)
particles:
cementite
(
Fe
3
C
)
(brittle)
60 mm
- WC/Co
cemented
carbide
matrix:
cobalt
(ductile)
particles:
WC
(brittle,
hard)
V
m
:
10-15 vol%
600 mm
- Automobile
tires
matrix:
rubber
(compliant)
particles:
C
(stiffer)
0.75 mm
Particle-reinforced
Fiber-reinforced
Structural

## Slide 8: Composite Survey: Particle-II
Concrete – gravel + sand + cement
  - Why sand and gravel? Sand packs into gravel voids
Reinforced concrete - Reinforce with steel rerod or remesh
    - increases strength - even if cement matrix is cracked
Prestressed concrete - remesh under tension during setting of concrete. Tension release puts concrete under compressive force
    - Concrete much stronger under compression.
    - Applied tension must exceed compressive force
Particle-reinforced
Fiber-reinforced
Structural
threaded
rod
nut
Post tensioning – tighten nuts to put under tension

## Slide 9: Victor Li: PVA-cement composites
Tough, rapid setting
cement-based materials
by incorporating polymer
fibers into mixture

## Slide 10: Composite Survey: Particle-III
• Elastic modulus, Ec, of composites:
-- two approaches.
• Application to other properties:
-- Electrical conductivity, se: Replace E in equations with se.
-- Thermal conductivity, k: Replace E in equations with k.
lower limit:
1
E
c
=
V
m
E
m
+
V
p
E
p
c
m
m
upper
limit:
E
=
V
E
+
V
p
E
p
“rule of mixtures”
Particle-reinforced
Fiber-reinforced
Structural
Data:
Cu matrix
w/tungsten
particles
0
20
4
0
6
0
8
0
10
0
150
20
0
250
30
0
350
vol% tungsten
E(GPa)
(Cu)
(
W)

## Slide 11: Composite Survey: Fiber-I
Fibers very strong
  Provide significant strength improvement to material
  Ex: fiber-glass
    Continuous glass filaments in a polymer matrix
    Strength due to fibers
    Polymer holds them in place
    Polyesters, polyimides, epoxies
Particle-reinforced
Fiber-reinforced
Structural

## Slide 12: Composite Survey: Fiber-II
Fiber Materials
  Whiskers - Thin single crystals - large length to diameter ratio
    graphite, SiN, SiC
    high crystal perfection – extremely strong, strongest known
    very expensive
Particle-reinforced
Fiber-reinforced
Structural
  Fibers
    polycrystalline or amorphous
    generally polymers or ceramics
    Ex: Al2O3 , Aramid, E-glass, Boron, UHMWPE, carbon
  Wires
    Metal – Steel, Mo, W

## Slide 13: Composite Survey: Fiber-III
• Aligned Continuous fibers
• Examples:
-- Metal: g'(Ni3Al)-a(Mo)
by eutectic solidification.
Particle-reinforced
Fiber-reinforced
Structural
matrix:
a
(Mo) (ductile)
fibers:
g
’ (Ni3Al) (brittle)
2 mm
-- Ceramic: Glass w/SiC fibers
formed by glass slurry
Eglass = 76 GPa; ESiC = 400 GPa.
(a)
(b)
fracture
surface

## Slide 14: Composite Survey: Fiber-IV
• Discontinuous, random 2D fibers
• Example: Carbon-Carbon
-- process: fiber/pitch, then
burn out at up to 2500ºC.
-- uses: disk brakes, gas
turbine exhaust flaps, nose
cones.
• Other variations:
-- Discontinuous, random 3D
glass in nylon or PP
-- Discontinuous, 1D
Particle-reinforced
Fiber-reinforced
Structural
(b)
fibers lie
in plane
view onto plane
C fibers:
very stiff
very
strong
C matrix:
less stiff
less strong
(a)

## Slide 15: Composite Survey: Fiber-V
• Critical fiber length for effective stiffening & strengthening:
• “Continuous” fibers when l > 15 lc
Particle-reinforced
Fiber-reinforced
Structural
fiber diameter
shear strength of
fiber-matrix interface
fiber strength in tension
• Why? Longer fibers carry stress more efficiently
Shorter, thicker fiber:
Longer, thinner fiber:
Poorer fiber efficiency
Better fiber efficiency
s
(x)
s
(x)
Typical L/D: 20-150

## Slide 16: Fiber Alignment
aligned
continuous
aligned random
discontinuous

## Slide 17: Composite Strength: Longitudinal Loading
Continuous fibers - Estimate fiber-reinforced composite strength for long continuous fibers in a matrix
Longitudinal deformation
c = mVm + fVf but c = m = f
  volume fraction isostrain
Ece = Em Vm + EfVf longitudinal (extensional)
      modulus
f = fiber
m = matrix

## Slide 18: Composite Strength: Transverse Loading
In transverse loading the fibers carry less of the load - isostress
  c = m = f =  c= mVm + fVf
transverse modulus


## Slide 19: Composite Strength
• Estimate of Ec for discontinuous fibers:
-- valid when
-- Elastic modulus in fiber direction:
efficiency factor:
-- aligned 1D: K = 1 (aligned )
-- aligned 1D: K = 0 (aligned )
-- random 2D: K = 3/8 (2D isotropy)
-- random 3D: K = 1/5 (3D isotropy)
Particle-reinforced
Fiber-reinforced
Structural
Ec = EmVm + KEfVf

## Slide 20: Composites Processing: Lay-Up
Lay fabric of reinforcement in layers
Pour in reinforcement over fibers in a container (open molding)
Contain object in a bag or two-sided mold, apply curing with temperature or crosslinking radiation (closed molding)
  electrons, light, X-rays

## Slide 21: Composite Production Methods-I
Pultrusion
  Continuous fibers pulled through resin tank, then preforming die & oven to cure

## Slide 22: Composite Production Methods-II
Filament Winding
  Ex: pressure tanks
  Continuous filaments wound onto mandrel

## Slide 23: Resin Transfer Molding: RTM
1: Cope 2: Drag 3: Clamp 4: Mixing chamber 5: Fiber preform
6: Heated mold 7: Resin 8: Curative
Can be done with Vacuum Assist: VARTM

## Slide 24: Common Defects in RTM

## Slide 25: Reinforced Reaction Injection Molding (RRIM)
Matrix: polyurethanes, polyureas (no reaction byproducts)
Reinforcement: glass fibers, mica, calcium carbonate
Products: bumpers, spoilers, fenders
Lower pressures (small molecules flow easier), but more expensive materials, somewhat slower than injection molding of polymer melts

## Slide 26: Composite Survey: Structural
• Stacked and bonded fiber-reinforced sheets
-- stacking sequence: e.g., 0º/90º
-- benefit: balanced, in-plane stiffness
Particle-reinforced
Fiber-reinforced
Structural
• Sandwich panels
-- low density, honeycomb core
-- benefit: small weight, large bending stiffness
honeycomb
adhesive layer
face sheet

## Slide 27: Composite Benefits
• CMCs: Increased toughness
fiber-reinf
un-reinf
particle-reinf
Force
Bend displacement
• PMCs: Increased E/r
E(GPa)
Density, r [mg/m3]
.1
.3
1
3
10
30
.01
.1
1
10
10
2
10
3
metal/
metal alloys
polymers
PMCs
ceramics
• MMCs:
Increased
creep
resistance
20
30
50
100
200
10
-10
10
-8
10
-6
10
-4
6061 Al
6061 Al
w/SiC
whiskers
s
(MPa)
e
ss
(s-1)

## Slide 28: Material property- charts: Modulus - Density
0.1
10
1
100
Metals
Polymers
Elastomers
Ceramics
Woods
Composites
Foams
0.01
1000
100
0.1
1
10
Density (Mg/m3)
Young’s modulus E, (GPa)
Unit 1, Frame 1.16
E/r (2)
E/r (1)

## Slide 29: Specfic Materials
Young’s modulus (GPa)
Density (Mg/m3)
Modulus - Density
Unit 1, Frame 1.18

## Slide 30: Specfic Materials
Young’s modulus (GPa)
Density (Mg/m3)
Modulus - Density
Unit 1, Frame 1.18

## Slide 31: Nanocomposites

## Slide 32: Composites at UD
Interdisciplinary Center for Composite Materials (CCM)
Students get degrees from partnering departments: MEEG, MSEG, CIEG, ChEG, BMEG, ELEG
Current director: Jack Gillespie
  MSEG, CIEG, MEEG
ccm.udel.edu

## Slide 33: CCM Research Areas
Materials and Synthesis
Mechanics and Design
Multifunctional Materials
Performance
Processing Science
Sensing and Control
Product Development
Engineering Services

## Slide 35: LaShanda Korley: CWRU -> UD
Bio-inspired Materials and Systems
  1) Silk-inspired Nanocomposites
  2) Spider / Caddisfly Silk Mimics
  3) Sea Cucumber, Squid Beak, and Pine Cone Inspired Adaptive Composites
  4) Dynamic and Functional Fibers Inspired by the Extracellular Matrix
  5) Soft Robotics Inspired by Worm Locomotion

## Slide 37: Summary
• Composites are classified according to:
-- the matrix material (CMC, MMC, PMC)
-- the reinforcement geometry (particles, fibers, layers).
• Composites enhance matrix properties:
-- MMC: enhance sy, TS, creep performance
-- CMC: enhance Kc
-- PMC: enhance E, sy, TS, creep performance
• Particulate-reinforced:
-- Elastic modulus can be estimated
-- Properties are isotropic
• Fiber-reinforced:
-- Elastic modulus and TS can be estimated along fiber dir.
-- Properties can be isotropic or anisotropic.
• Structural:
-- Based on build-up of sandwiches in layered form