## Slide 1: CHAPTER 4: IMPERFECTIONS IN SOLIDS
ISSUES TO ADDRESS...
• What types of defects arise in solids?
• Can the number and type of defects be varied
and controlled?
• How do defects affect material properties?
• Are defects undesirable?
• What are the solidification mechanisms?

## Slide 2: Imperfections in Solids
Many of the important properties of materials are due to the presence of imperfections, or defects. Anything that disrupts the symmetry of the material is by definition a defect. Defects in materials are not necessarily bad.
What are these imperfections?
Why are they important?

## Slide 3: Types of Imperfections in Crystals
Vacancy atoms
Interstitial atoms
Substitutional atoms
Point defects
Dislocations
Line defects
Grain Boundaries
Surfaces
Area defects

## Slide 5: Imperfections in Solids
Solidification- result of casting of molten material
  2 steps
    Nuclei form
    Nuclei grow to form crystals – grain structure
Start with a molten material – all liquid
Crystals grow until they meet each other
nuclei
crystals growing
grain structure
liquid

## Slide 6: Nucleating Agents: Water -> Snow
“Surprisingly, the use of dirty water or water containing crushed ice results in more efficient operation, whereby the dirt and ice particles serve as crystallizing nuclei thereby aiding in the formation of snow crystals.”

## Slide 7: Crystal Nucleating Agents

## Slide 8: Solidification
Columnar in area with less undercooling
Shell of equiaxed grains due to rapid cooling (greater T) near wall
Grain refiner - added to make smaller, more uniform, equiaxed grains.
heat
flow
Grains can be - equiaxed (roughly same size in all directions)
  - columnar (elongated grains)
~ 8 cm

## Slide 9: Polycrystalline Materials
Grain Boundaries
regions between crystals
transition from lattice of one region to that of the other
slightly disordered
low density in grain boundaries
  high mobility
  high diffusivity
  high chemical reactivity

## Slide 10: Planar Defects in Solids
One case is a twin boundary (plane)
  Essentially a reflection of atom positions across the twin plane.
Stacking faults
  For FCC metals an error in ABCABC packing sequence
  Ex: ABCABABC

## Slide 11
Point Defects

## Slide 12: Point Defects
• Vacancies:
-vacant atomic sites in a structure.
• Self-Interstitials:
-"extra" atoms positioned between atomic sites.
Vacancy
distortion
of planes
self-
interstitial
distortion
of planes

## Slide 13
Point Defects in Ionic Crystals

## Slide 14: Importance of point defects
Solid-state diffusion (Chapter 5)
Mechanical properties (carbon in iron)
Electrical properties in semiconductors
Color
Al2O3: alumina, corundum (trigonal crystal structure)
+Chromium  ruby (red)
+Titanium, Iron,…  sapphire (not red: blue, orange, …)

## Slide 15: Equilibrium Concentration: Point Defects
Boltzmann's constant
(1.38 x 10
-23
J/atom-K)
(8.62
x
10
-5
eV/atom-K)
ç
N
v
N
=
exp
-
Q
v
k
T
æ
è
ç
ö
ø
No. of defects
No. of potential
defect sites.
Activation energy
Temperature
Each lattice site
is a potential
vacancy site
• Equilibrium concentration varies with temperature

## Slide 16: Measuring Activation Energy
• We can get Qv from
an experiment.
ç
N
v
N
=
exp
-
Q
v
k
T
æ
è
ç
ö
ø
• Measure this...
N
v
N
T
exponential
dependence!
defect concentration
• Replot it...
1/
T
N
N
v
ln
-
Q
v
/k
slope

## Slide 17
Q: how is Nv actually measured?
Need careful measurements of thermal expansion:
As well as careful measurements of lattice expansion
)
Effect is small (Nv low relative to N), so experiments
require accuracy of 1/100,000, must be done at same time
(dilatometry)
(X-ray diffraction)
Simmons and Balluffi, Phys. Rev., 117, 52, (1960).

## Slide 18: Estimating Vacancy Concentration
• Find the equil. # of vacancies in 1 m3 of Cu at 1000C.
• Given:
A
Cu
= 63.5 g/mol
r
= 8.4 g
/
cm
3
Q
v
= 0.9 eV/atom
N
A
= 6.02 x 1023
atoms/mol
For 1 m3
, N =
N
A
A
Cu
r
x
x
1 m3
= 8.0 x 1028 sites
8.62 x 10-5
eV/atom-K
0.9 eV/atom
1273K
ç
N
v
N
=
exp
-
Q
v
k
T
æ
è
ç
ö
ø
= 2.7 x 10-4
• Answer:
N
v
=
(2.7 x 10-4)(8.0 x 1028) sites = 2.2 x 1025 vacancies

## Slide 19: Point Defects in Alloys
Two outcomes if impurity (B) added to host (A):
• Solid solution of B in A (i.e., random dist. of point defects)
• Solid solution of B in A plus particles of a new
phase (usually for a larger amount of B)
OR
Substitutional solid soln.
(e.g., Cu in Ni)
Interstitial solid soln.
(e.g., C in Fe)
Second phase particle
--different composition
--often different structure.

## Slide 20: Imperfections in Solids
Specification of composition
  weight percent
m1 = mass of component 1
nm1 = number of moles of component 1
atom percent
Vm1 = volume of component 1 = m1/r1
volume percent

## Slide 21: Line Defects
• are line defects,
• slip between crystal planes result when dislocations move,
• produce permanent (plastic) deformation.
Dislocations:
Schematic of Zinc (HCP):
• before deformation
• after tensile elongation
slip steps

## Slide 22: Imperfections in Solids
Linear Defects (Dislocations)
  Are one-dimensional defects around which atoms are misaligned
Edge dislocation:
  extra half-plane of atoms inserted in a crystal structure
  b  to dislocation line
Screw dislocation:
  spiral planar ramp resulting from shear deformation
  b  to dislocation line
Burger’s vector, b: measure of lattice distortion

## Slide 23: Imperfections in Solids
Edge Dislocation

## Slide 24: Motion of Edge Dislocation
• Dislocation motion requires the successive bumping
of a half plane of atoms (from left to right here).
• Bonds across the slipping planes are broken and
remade in succession.
Atomic view of edge
dislocation motion from
left to right as a crystal
is sheared.

## Slide 25: Imperfections in Solids
Screw Dislocation
Burgers vector b
Dislocation
line
b
(a)
(b)
Screw Dislocation

## Slide 26: Screw Dislocation
In VMSE on wileyplus:
  a region of crystal containing a dislocation can be rotated in 3D
  dislocation motion may be animated
Front View
Top View
VMSE Screen Shots

## Slide 27: Edge, Screw, and Mixed Dislocations
Edge
Screw
Mixed

## Slide 28: https://youtu.be/JPVS8d2c_4U
Screw Dislocation Motion in CaO
Paulo Branicio, USC
https://youtu.be/VLsLS74AM9o
Dislocations can
dissociate into
two partials and
a stacking fault
https://youtu.be/1r-UqxmuYCw
Bragg, 1947, bubbles:
Needle in particles:

## Slide 29
Why dissociate into partials?
Dislocation energy is proportional to Gb2
Full dislocation  Two partials + stacking fault
Gb2  G(b/2)2 + gf + G(b/2)2
If equal, f = Gb2/2g or g = Gb2/2f
If g small, partials will separate widely (f large)

## Slide 30: Surface Energy
Some values of surface energy: mN/m or dyn/cm
Hexane
Substance | Surface tension
Hexane | 18.4
Ethanol | 22.3
Acetic acid | 27.6
Water | 72
Mercury | 487
Carbon | 3700

## Slide 32: Low angle gbs: dislocation arrays

## Slide 33: Grain Boundaries

## Slide 34: Grain boundary energies

## Slide 35: Steps and Kinks

## Slide 36: Surface reconstructions

## Slide 37: Si (001)

## Slide 38: Si (111) 7x7 reconstruction

## Slide 39: Si (111) 7x7 reconstruction

## Slide 40: Imperfections in Solids
Dislocations are visible in electron micrographs: TEM
Looking down on
the top of a thin
metal film
Dislocations are the
dark lines, running
mostly from top to
bottom of the film

## Slide 41: Dislocations, Slip Planes, & Crystal Structures
• Structure: close-packed
planes & directions
are preferred.
view onto two
close-packed
planes.
close-packed plane (bottom)
close-packed plane (top)
close-packed directions
• Comparison among crystal structures:
FCC: many close-packed planes (111)/directions [110];
HCP: only one (basal) plane, 3 directions;
BCC: none
• Specimens that
were tensile
tested.
Mg (HCP)
Al (FCC)
tensile direction

## Slide 42: Catalysts and Surface Defects
A catalyst increases the rate of a chemical reaction without being consumed
Active sites on catalysts are normally surface defects
Fig. 4.11, Callister & Rethwisch 9e.
Fig. 4.12, Callister & Rethwisch 9e.
[From W. J. Stark, L. Mädler, M. Maciejewski, S. E. Pratsinis, and A. Baiker, “Flame Synthesis of Nanocrystalline Ceria/Zirconia: Effect of Carrier Liquid,” Chem. Comm., 588–589 (2003). Reproduced by permission of The Royal Society of Chemistry.]
Single crystals of (Ce0.5Zr0.5)O2 used in an automotive catalytic converter

## Slide 44: Changing grain size: additives (refiners)
Left: pure aluminum. Right: +0.2% Al-5Ti-1B refiner

## Slide 45: Effects on properties: Yield Stress
Grain boundaries cause dislocation pile-up
For larger grains, metals
get harder when grain size d
gets smaller
Hall-Petch equation

## Slide 46: When grains are really small (~10 nm) the material softens (g.b. sliding?)
Xiao et al., (2015): DOI: 10.1098/rspa.2014.0832
FCC Copper

## Slide 47: Small amounts of impurities (dopants) added to crystalline, semiconducting silicon dramatically changes electrical properties
n-doping:
electrons
p-doping
holes

## Slide 48: Field-Effect Transistor
A small voltage
change on the gate
dramatically changes
current flow from
source to drain
Electronic valve:
can be open, closed
Can be used as
an amplifier, logic gate,
memory

## Slide 49: Understanding Defects: Microscopic Examination
Crystallites (grains) and grain boundaries. Vary considerably in size. Can be quite large
  ex: Large single crystal of quartz or diamond or Si
  ex: Aluminum light post or garbage can - see the individual grains
Crystallites (grains) can be quite small (mm or less) – necessary to observe with a microscope.

## Slide 50: Optical Microscopy
• Useful up to 2000X magnification (~1 mm).
• Polishing removes surface features (e.g., scratches)
• Etching changes reflectance, depending on crystal
orientation.
Micrograph of
brass (a Cu-Zn alloy)
0.75mm
crystallographic planes

## Slide 51: Optical Microscopy
Grain boundaries...
• are imperfections,
• are more susceptible
to etching,
• may be revealed as
dark lines,
• change in crystal
orientation across
boundary.
ASTM grain
size number
n
= 2
G
-1
number of grains/in2
at 100x
magnification
Fe-Cr alloy
(b)
grain boundary
surface groove
polished surface
(a)

## Slide 52
ASTM E 112-13
Standard for Determining Average Grain Size
Image analysis software: ImageJ from NIH

## Slide 54: Optical Microscopy
Polarized light
  metallographic scopes often use polarized light to increase contrast
  Also used for transparent samples such as polymers

## Slide 55: Microscopy
Optical resolution ca. 10-6 m = 1 m = 1000 nm
  Wavelength of visible light: 400-700 nm
For higher resolution need small wavelengths
  X-Rays? Wavelength: Cu Ka 0.154 nm (1.54 Ang)
    Difficult to focus, scattering OK
  Electrons
    Electron beam focused by magnetic lenses
    Voltages 5 kV : 100-400 kV : 1 MV
    Wavelengths ~ 3 pm (0.003 nm)
      Magnifications - 1,000,000X
    Atomic resolution possible… approaching 0.05 nm (0.5 Ang)
    Scanning EM (SEM): 1 kV – 30 kV
    Transmission EM (TEM) : 200-400 kV
    STEM
Notes: Optical microscopy good to ca. wavelength of light
Higher frequencies
X-rays – good idea but difficult to focus
Electrons - wavelength proportional to velocity with high voltage (high acceleration) get wavelengths ca. 3pm (0.003nm) (x1,000,000)

## Slide 56: Scanned Probe Microscopies: Scanning Tunneling Microscopy (STM) Atomic Force Microscopy (AFM)
• Atoms can be arranged and imaged!
Carbon monoxide molecules arranged on a platinum (111) surface.
Iron atoms arranged on a copper (111) surface. These Kanji characters represent the word “atom”.

## Slide 57
http://www.princeton.edu/~kahnlab/STMImages.
http://www.nisenet.org/publicbeta/articles/seeing_atoms/index.html

## Slide 59
Zeiss Auriga 60 FIB/SEM
JEOL JSM-7400F SEM
FEI / ThermoSci Talos 200C STEM
JEOL JEM-3010 TEM
JEOL JEM-2010F STEM
FEI / ThermoSci Technai G2 12 TEM

## Slide 60
https://www.quora.com/What-is-the-difference-between-the-SEM-microscope-and-the-STEM-microscope

## Slide 62
X-ray Diffraction
Thermal Analysis
Porosity and Particle Size Analysis
Vibrational Spectroscopy
Mass Spectroscopy
http://sites.udel.edu/amcl/

## Slide 63: Summary
• Point, Line, and Area defects exist in solids.
• The number and type of defects can be varied
and controlled (e.g., T controls vacancy conc.)
• Defects affect material properties (e.g., grain
boundaries control crystal slip).
• Defects may be desirable or undesirable
(e.g., dislocations may be good or bad, depending
on whether plastic deformation is desirable or not)

## Slide 64: Imperfections in Solids
Conditions for substitutional solid solution (S.S.)
W. Hume – Rothery rules
  1. r (atomic radius) < 15%
  2. Proximity in periodic table
    i.e., similar electronegativities
  3. Same crystal structure for pure metals
  4. Valency
    All else being equal, a metal will have a greater tendency to dissolve a metal of higher valency than one of lower valency

## Slide 65: Imperfections in Solids
Application of Hume–Rothery rules – Solid Solutions
1. Would you predict more Al or Ag to dissolve in Zn?
2. More Zn or Al
in Cu?
Element Atomic Crystal Electro- Valence Radius Structure nega- (nm) tivity
Cu 0.1278 FCC 1.9 +2 C 0.071 H 0.046 O 0.060 Ag 0.1445 FCC 1.9 +1 Al 0.1431 FCC 1.5 +3 Co 0.1253 HCP 1.8 +2 Cr 0.1249 BCC 1.6 +3 Fe 0.1241 BCC 1.8 +2 Ni 0.1246 FCC 1.8 +2 Pd 0.1376 FCC 2.2 +2 Zn 0.1332 HCP 1.6 +2