## Slide 1: Materials Selection
MSEG 302 Spring 2018

## Slide 2: The world of materials
PE, PP, PC
PA (Nylon)
Polymers,
elastomers
Butyl rubber
Neoprene
Polymer foams
Metal foams
Foams
Ceramic foams
Glass foams
Woods
Natural
materials
Natural fibres:
Hemp, Flax,
Cotton
GFRP
CFRP
Composites
KFRP
Plywood
Alumina
Si-Carbide
Ceramics,
glasses
Soda-glass
Pyrex
Steels
Cast irons
Al-alloys
Metals
Cu-alloys
Ni-alloys
Ti-alloys
Unit 1, Frame 1.4

## Slide 3: Mechanical properties illustrated
Stiff
Strong
Tough
Light
Not stiff enough (need bigger E)
Not strong enough (need bigger y )
Not tough enough (need bigger Kic)
Too heavy (need lower )
All OK !
Unit 1, Frame 1.6

## Slide 4: Basic material properties
General
Weight: Density , Mg/m3
Expense: Cost/kg Cm, $/kg
Mechanical
Stiffness: Young’s modulus E, GPa
Strength: Elastic limit y , MPa
Fracture strength: Tensile strength ts , MPa
Brittleness: Fracture toughness Kic , MPa.m1/2
Thermal
Expansion: Expansion coeff. , 1/K
Conduction: Thermal conductivity , W/m.K
Electrical
Conductor? Insulator?
Young’s modulus, E
Elastic limit,
Strain
Stress 
Ductile materials
Brittle materials
Young’s
modulus, E
Tensile (fracture)
strength,
Strain
Stress 


Thermal expansion
Expansion
coefficient, 
Temperature, T
Thermal strain 
T1
To
Q joules/sec
x
Area A
Thermal conduction
Mechanical properties
Thermal
conductivity, 
(T1 -T0)/x
Heat flux, Q/A
Unit 1, Frame 1.5

## Slide 5: Material property- charts: Modulus - Density
0.1
10
1
100
Metals
Polymers
Elastomers
Ceramics
Woods
Composites
Foams
0.01
1000
100
0.1
1
10
Density (Mg/m3)
Young’s modulus E, (GPa)
Unit 1, Frame 1.16

## Slide 6
Young’s modulus (GPa)
Density (g/cm3)
Modulus - Density
Unit 1, Frame 1.18

## Slide 7
Conductivity -
Expansion
Thermal expansion (10-6/K)
Thermal conductivity (W/m.K)
Unit 1, Frame 1.20

## Slide 8: Optimised selection
For beam bending,
Contours of constant
C are lines of slope 2
on an E- chart
0.1
10
1
100
Metals
Polymers
Elastomers
Woods
Composites
Foams
0.01
1000
100
0.1
1
10
Density (Mg/m3)
Young’s modulus E, (GPa)
Ceramics
1
2
3
tension
beam
panel

## Slide 9
Density (Mg/m3)
Young’s modulus (GPa)
Unit 2, Frame 2.15
Search
area

## Slide 10
Density (Mg/m3)
Young’s modulus (GPa)
Unit 2, Frame 2.15
Oars: real life
Wood: Sitka spruce, quartered and laminated
CFRP: Tailored to rower’s specification

## Slide 11: Bionic Devices in Science Fiction
http://www.youtube.com/watch?v=HofoK_QQxGc
Steve Austin, 1974
Luke Skywalker, 1980
1972
1984

## Slide 12: Integrated Bionic Prosthesis
Former U. S. Marine Claudia Mitchell: http://www.youtube.com/

## Slide 13
CyberKinetics
Implantable
glucose
sensor +
insulin pump
Bionic devices: solid electronic wire – wet ionic tissue interfaces
Michigan CNCT
NeuroNexus
Second Sight Retinal Implant
DBS electrode
Cochlear Electrode
Utah MEA

## Slide 14
Second Sight: 2-sight.eu

## Slide 16: Electrode-Tissue Interfaces
Major Road Blocks
Foreign body reaction
Device biofouling, eventual failure
Signal blocking glial scar/encapsulation
Loss of proximal neurons
Biomaterials Design
Mechanical Properties
  Hard to Soft
Bioactivity
  Inert to Living
Electronic Transport
  Electronic to Ionic
Surface Topography
  Flat to Articulated
Permeability
  Solid to Wet Network

## Slide 17
Abiotic Devices : Conjugated Polymers : Living Tissue

## Slide 18: Modulus-Resistivity Map
CES Selector 4.6.1, Granta Design, (2006)
Resistivity (Ohm-meters)
Stiff
Insulating
Stiff
Conducting
Soft
Insulating
Soft
Conducting

## Slide 19: Modulus-Resistivity Map
CES Selector 4.6.1, Granta Design, (2006)
Resistivity (Ohm-meters)
Stiff
Insulating
Stiff
Conducting
Soft
Insulating
Soft
Conducting
Wires
Plastic
Bottles
Rubber
Bands
Foam
Cushions
Rocks
Computer
Chips

## Slide 20: Modulus-Resistivity Map
CES Selector 4.6.1, Granta Design, (2006)
Tissue
Resistivity (Ohm-meters)
Stiff
Insulating
Stiff
Conducting
Soft
Insulating
Soft
Conducting
Wires
Plastic
Bottles
Rubber
Bands
Foam
Cushions
Rocks
Computer
Chips

## Slide 21: Modulus-Resistivity Map
CES Selector 4.6.1, Granta Design, (2006)
Tissue
Resistivity (Ohm-meters)
PEDOT
Stiff
Insulating
Stiff
Conducting
Soft
Insulating
Soft
Conducting
Wires
Plastic
Bottles
Rubber
Bands
Foam
Cushions
Rocks
Computer
Chips

## Slide 22: Modulus-Resistivity Map
CES Selector 4.6.1, Granta Design, (2006)
Tissue
Resistivity (Ohm-meters)
PEDOT in Gels, Tissue
PEDOT
Stiff
Insulating
Stiff
Conducting
Soft
Insulating
Soft
Conducting
Wires
Plastic
Bottles
Rubber
Bands
Foam
Cushions
Rocks
Computer
Chips