## Slide 1: Chapter 8: Mechanical Failure
ISSUES TO ADDRESS...
• How do flaws in a material initiate failure?
• How is fracture resistance quantified; how do different
material classes compare?
• How do we estimate the stress to fracture?
• How do loading rate, loading history, and temperature
affect the failure stress?
Ship-cyclic loading
from waves.
Computer chip-cyclic
thermal loading.
Hip implant-cyclic
loading from walking.

## Slide 2: Fracture mechanisms
Ductile fracture
  Occurs with plastic deformation
Brittle fracture
  Little or no plastic deformation
  Catastrophic

## Slide 3: Ductile vs Brittle Failure
Very
Ductile
Moderately
Ductile
Brittle
Fracture
behavior:
Large
Moderate
%AR or %EL
Small
• Ductile
fracture is usually
desirable!
• Classification:
Ductile:
warning before fracture
Brittle: No warning

## Slide 4: Example: Failure of a Pipe
• Ductile failure:
--one piece
--large deformation
• Brittle failure:
--many pieces
--small deformation

## Slide 5: Moderately Ductile Failure
• Evolution to failure:
• Resulting
fracture
surfaces
(steel)
50 mm
particles
serve as void
nucleation
sites.
50 mm
100 mm
Fracture surface of tire cord wire loaded in tension. Courtesy of F. Roehrig, CC Technologies, Dublin, OH. Used with permission.
necking
s
void
nucleation
void growth
and linkage
shearing
at surface
fracture

## Slide 6: Ductile vs. Brittle Failure
cup-and-cone fracture
brittle fracture

## Slide 7: Brittle Failure
Arrows indicate pt at which failure originated

## Slide 8: Brittle Fracture Surfaces
• Intergranular
(between grains)
• Intragranular
(within grains)
Al Oxide
(ceramic)
Reprinted w/ permission from "Failure Analysis of Brittle Materials", p. 78. Copyright 1990, The American Ceramic Society, Westerville, OH. (Micrograph by R.M. Gruver and H. Kirchner.)
316 S. Steel (metal)
Reprinted w/ permission from "Metals Handbook", 9th ed, Fig. 650, p. 357. Copyright 1985, ASM International, Materials Park, OH. (Micrograph by D.R. Diercks, Argonne National Lab.)
304 S. Steel (metal)
Reprinted w/permission from "Metals Handbook", 9th ed, Fig. 633, p. 650. Copyright 1985, ASM International, Materials Park, OH. (Micrograph by J.R. Keiser and A.R. Olsen, Oak Ridge National Lab.)
Polypropylene
(polymer)
Reprinted w/ permission from R.W. Hertzberg, "Deformation and Fracture Mechanics of Engineering Materials", (4th ed.) Fig. 7.35(d), p. 303, John Wiley and Sons, Inc., 1996.
3 mm
4 mm
160 mm
1 mm
(Orig. source: K. Friedrick, Fracture 1977, Vol. 3, ICF4, Waterloo, CA, 1977, p. 1119.)

## Slide 9: Ideal vs Real Materials
• Stress-strain behavior (Room T):
TS << TS
engineering
materials
perfect
materials
s
e
E/10
E/100
0.1
perfect mat’l-no flaws
carefully produced glass fiber
typical ceramic
typical strengthened metal
typical polymer
• DaVinci (500 yrs ago!) observed...
-- the longer the wire, the
smaller the load for failure.
• Reasons:
-- flaws cause premature failure.
-- Larger samples contain more flaws!
Reprinted w/ permission from R.W. Hertzberg, "Deformation and Fracture Mechanics of Engineering Materials", (4th ed.) Fig. 7.4. John Wiley and Sons, Inc., 1996.

## Slide 10: Concentration of Stress at Crack Tip
s0

## Slide 11: Flaws are Stress Concentrators!
Results from crack propagation
Griffith Crack
where t = radius of curvature
so = applied stress
sm = stress at crack tip
t
Adapted from Fig. 8.8(a), Callister 7e.
Notes: Stress concentrated at crack tip

## Slide 12: Engineering Fracture Design
r/h
sharper fillet radius
increasing
w/h
0
0.5
1.0
1.0
1.5
2.0
2.5
Stress Conc. Factor, K
t
s
max
s
o
=
• Avoid sharp corners!
s
Adapted from Fig. 8.2W(c), Callister 6e.
(Fig. 8.2W(c) is from G.H. Neugebauer, Prod. Eng. (NY), Vol. 14, pp. 82-87 1943.)
r ,
fillet
radius
w
h
o
s
max

## Slide 13: Crack Propagation
Cracks propagate due to sharpness of crack tip
A plastic material deforms at the tip, “blunting” the crack.
deformed region
    brittle
Energy balance on the crack
Elastic strain energy-
    energy stored in material as it is elastically deformed
    this energy is released when the crack propagates
    creation of new surfaces requires energy
plastic

## Slide 14: When Does a Crack Propagate?
Crack propagates if above critical stress
where
  E = modulus of elasticity
  s = specific surface energy
  a = one half length of internal crack
  Kc = sc/s0
For ductile => replace gs by gs + gp
  where gp is plastic deformation energy
i.e., sm > sc
or Kt > Kc

## Slide 15: Fracture Toughness
• Crack growth condition:
Kc: fracture toughness, has units of MPa m1/2
: applied stress (MPa)
a: crack length (m)
Y: dimensionless parameter, may be function of a

## Slide 16
Crack Displacement Modes
I
tensile
II
sliding
III
tearing

## Slide 18: Fracture Toughness
Based on data in Table B5,
Callister 7e.
Composite reinforcement geometry is: f = fibers; sf = short fibers; w = whiskers; p = particles. Addition data as noted (vol. fraction of reinforcement):
1. (55vol%) ASM Handbook, Vol. 21, ASM Int., Materials Park, OH (2001) p. 606.
2. (55 vol%) Courtesy J. Cornie, MMC, Inc., Waltham, MA.
3. (30 vol%) P.F. Becher et al., Fracture Mechanics of Ceramics, Vol. 7, Plenum Press (1986). pp. 61-73.
4. Courtesy CoorsTek, Golden, CO.
5. (30 vol%) S.T. Buljan et al., "Development of Ceramic Matrix Composites for Application in Technology for Advanced Engines Program", ORNL/Sub/85-22011/2, ORNL, 1992.
6. (20vol%) F.D. Gace et al., Ceram. Eng. Sci. Proc., Vol. 7 (1986) pp. 978-82.
Graphite/
Ceramics/
Semicond
Metals/
Alloys
Composites/
fibers
Polymers
5
K
Ic
(MPa · m
0.5
)
1
Mg alloys
Al alloys
Ti alloys
Steels
Si crystal
Glass
-
soda
Concrete
Si carbide
PC
Glass
6
0.5
0.7
2
4
3
10
2
0
3
0
<100>
<111>
Diamond
PVC
PP
Polyester
PS
PET
C-C
(|| fibers)
1
0.6
6
7
4
0
5
0
6
0
7
0
100
Al oxide
Si nitride
C/C
( fibers)
1
Al/Al oxide(sf)
2
Al oxid/SiC(w)
3
Al oxid/ZrO
2
(p)
4
Si nitr/SiC(w)
5
Glass/SiC(w)
6
Y
2
O
3
/ZrO
2
(p)
4

## Slide 20: Design Against Crack Growth
• Crack growth condition:
• Largest, most stressed cracks grow first!
K ≥ Kc =
--Result 1: Max. flaw size
dictates design stress.
s
amax
no
fracture
fracture
--Result 2: Design stress
dictates max. flaw size.
amax
s
no
fracture
fracture

## Slide 21: Design Example: Aircraft Wing
• Two designs to consider...
Design A
--largest flaw is 9 mm
--failure stress = 112 MPa
Design B
--use same material
--largest flaw is 4 mm
--failure stress = ?
• Key point: Y and Kc are the same in both designs.
Answer:
• Reducing flaw size pays off!
• Material has Kc = 26 MPa-m0.5
• Use...
9 mm
112 MPa
4 mm
--Result:

## Slide 22: Loading Rate
• Increased loading rate...
-- increases sy and TS
-- decreases %EL
• Why? An increased rate
gives less time for
dislocations to move past
obstacles.
s
e
sy
sy
TS
TS
larger
e
smaller
e

## Slide 23: Impact Testing
final height
initial height
• Impact loading:
-- severe testing case
-- makes material more brittle
-- decreases toughness
(Charpy)

## Slide 24: Temperature
• Increasing temperature...
--increases %EL and Kc
• Ductile-to-Brittle Transition Temperature (DBTT)...
BCC metals (e.g., iron at T < 914°C)
Impact Energy
Temperature
High strength materials (
s
y
> E/150)
polymers
More Ductile
Brittle
Ductile-to-brittle
transition temperature
FCC metals (e.g., Cu, Ni)

## Slide 25: Design Strategy: Stay Above The DBTT!
• Pre-WWII: The Titanic
• WWII: Liberty ships
• Problem: Used a type of steel with a DBTT ~ Room temp.
Reprinted w/ permission from R.W. Hertzberg, "Deformation and Fracture Mechanics of Engineering Materials", (4th ed.) Fig. 7.1(a), p. 262, John Wiley and Sons, Inc., 1996. (Orig. source: Dr. Robert D. Ballard, The Discovery of the Titanic.)
Reprinted w/ permission from R.W. Hertzberg, "Deformation and Fracture Mechanics of Engineering Materials", (4th ed.) Fig. 7.1(b), p. 262, John Wiley and Sons, Inc., 1996. (Orig. source: Earl R. Parker, "Behavior of Engineering Structures", Nat. Acad. Sci., Nat. Res. Council, John Wiley and Sons, Inc., NY, 1957.)

## Slide 26: Fatigue
• Fatigue = failure under cyclic stress.
• Stress varies with time.
-- key parameters are S, sm, and frequency
s
max
s
min
s
time
s
m
S
• Key points: Fatigue...
--can cause part failure, even though smax < sc.
--causes ~ 90% of mechanical engineering failures.
tension on bottom
compression on top
counter
motor
flex coupling
specimen
bearing
bearing

## Slide 27: Fatigue Design Parameters
• Fatigue limit, Sfat:
--no fatigue if S < Sfat
Adapted from Fig. 8.19(a), Callister 7e.
Sfat
case for
steel
(typ.)
N = Cycles to failure
10
3
10
5
10
7
10
9
unsafe
safe
S = stress amplitude
• Sometimes, the
fatigue limit is zero!
Adapted from Fig. 8.19(b), Callister 7e.
case for
Al
(typ.)
N = Cycles to failure
10
3
10
5
10
7
10
9
unsafe
safe
S = stress amplitude

## Slide 29: Fatigue Mechanism
• Crack grows incrementally
typ. 1 to 6
increase in crack length per loading cycle
• Failed rotating shaft
--crack grew even though
Kmax < Kc
--crack grows faster as
• Ds increases
• crack gets longer
• loading freq. increases.
crack origin
Adapted from
Fig. 8.21, Callister 7e. (Fig. 8.21 is from D.J. Wulpi, Understanding How Components Fail, American Society for Metals, Materials Park, OH, 1985.)

## Slide 30
In region II: da/dN = C (DK)m
Fatigue Crack Propagation

## Slide 31: Improving Fatigue Life
1. Impose a compressive
surface stress
(to suppress surface
cracks from growing)
N = Cycles to failure
moderate tensile
s
m
Larger tensile
s
m
S = stress amplitude
near zero or compressive
s
m
Increasing m
--Method 1: shot peening
put
surface
into
compression
shot
--Method 2: carburizing
C-rich gas
2. Remove stress
concentrators.
Adapted from
Fig. 8.25, Callister 7e.
bad
bad
better
better

## Slide 32: Creep
Sample deformation at a constant stress (s) vs. time
Adapted from
Fig. 8.28, Callister 7e.
Primary Creep: slope (creep rate) decreases with time.
Secondary Creep: steady-state i.e., constant slope.
Tertiary Creep: slope (creep rate) increases with time, i.e. acceleration of rate.
s
s,e
0
t

## Slide 33: Creep
• Occurs at elevated temperature, T > 0.4 Tm
elastic
primary
secondary
tertiary

## Slide 34: Secondary Creep
• Strain rate is constant at a given T, s
-- strain hardening is balanced by recovery
stress exponent (material parameter)
strain rate
activation energy for creep
(material parameter)
applied stress
material const.
• Strain rate
increases
for higher T, s
10
2
0
4
0
10
0
2
0
0
10
-2
10
-1
1
Steady state creep rate (%/1000hr)
e
s
Stress (MPa)
427°C
538
°C
649
°C
Adapted from
Fig. 8.31, Callister 7e.
(Fig. 8.31 is from Metals Handbook: Properties and Selection: Stainless Steels, Tool Materials, and Special Purpose Metals, Vol. 3, 9th ed., D. Benjamin (Senior Ed.), American Society for Metals, 1980, p. 131.)

## Slide 35: Creep Failure
• Estimate rupture time
S-590 Iron, T = 800°C, s = 20 ksi
• Failure:
along grain boundaries.
time to failure (rupture)
function of
applied stress
temperature
applied
stress
g.b. cavities
• Time to rupture, tr
From V.J. Colangelo and F.A. Heiser, Analysis of Metallurgical Failures (2nd ed.), Fig. 4.32, p. 87, John Wiley and Sons, Inc., 1987. (Orig. source: Pergamon Press, Inc.)
1073K
Ans: tr = 233 hr
24x103 K-log hr
Adapted from
Fig. 8.32, Callister 7e.
(Fig. 8.32 is from F.R. Larson and J. Miller, Trans. ASME, 74, 765 (1952).)
L(10
3
K-log hr)
Stress, ksi
100
10
1
12
20
24
28
16
data for
S-590 Iron
20

## Slide 36: SUMMARY
• Engineering materials don't reach theoretical strength.
• Flaws produce stress concentrations that cause
premature failure.
• Sharp corners produce large stress concentrations
and premature failure.
• Failure type depends on T and stress:
- for noncyclic s and T < 0.4Tm, failure stress decreases with:
- increased maximum flaw size,
- decreased T,
- increased rate of loading.
- for cyclic s:
- cycles to fail decreases as Ds increases.
- for higher T (T > 0.4Tm):
- time to fail decreases as s or T increases.