## Slide 1: CHAPTER 14: POLYMER STRUCTURES
ISSUES TO ADDRESS...
• What are the basic microstructural features?
• How are polymer properties effected by
molecular weight?
• How do polymeric crystals accommodate the
polymer chain?
• How does crystallinity impact properties?

## Slide 2: Chapter 14 – Polymers
What is a polymer?
Poly mer
        many repeat unit
C
C
C
C
C
C
H
H
H
H
H
H
H
H
H
H
H
H
Polyethylene (PE)
Cl
Cl
Cl
C
C
C
C
C
C
H
H
H
H
H
H
H
H
H
Polyvinyl chloride (PVC)
H
H
H
H
H
H
Polypropylene (PP)
C
C
C
C
C
C
CH3
H
H
CH3
CH3
H
repeat
unit
repeat
unit
repeat
unit

## Slide 3: Polymers common in nature
  Wood: cellulose, lignin
  Rubber: polyisoprene
  Cotton: cellulose
  Wool, feathers, fingernails: keratin
  Silk: silk protein
  Leather: collagen protein
  Shellac: polyesters
Polymers can also be created from a variety of
other molecules; petroleum byproducts
(ethylene, propylene, styrene) are
particularly inexpensive

## Slide 4: Polymer Composition
Some polymers are hydrocarbons
– i.e. made up of only H and C
Saturated hydrocarbons
  Each carbon bonded to four other atoms
  CnH2n+2

## Slide 6: Molecular weights
Hydrocarbons: CnH2n+2
liquid
gas
solid

## Slide 7: Tailoring properties with chemistry

## Slide 8: Isomerism
Isomerism
  two compounds with same chemical formula can have quite different structures
  Ex: C8H18
    n-octane
    2-methyl-4-ethyl pentane (isooctane)


## Slide 9: Organic Chemistry shorthand
C4H10O

## Slide 10: Unsaturated Hydrocarbons
Double & triple bonds relatively reactive – can form new bonds
  Double bond – ethylene or ethene - CnH2n
    4-bonds, but only 3 atoms bound to C’s
  Triple bond – acetylene or ethyne - CnH2n-2

## Slide 11: Shorthand structures

## Slide 12: Chemistry of Polymers
Note: polyethylene is just a long HC
  - paraffin is short polyethylene
Notes:   Polymer- can have various lengths depending on number of repeat units

## Slide 13: Chemistry of Polymers: Chain Growth
Free radical polymerization
Initiator: example - benzoyl peroxide

## Slide 14: Step-Growth (Condensation) Polymerization
React diacid (A-A) with dibase (B-B)
React A-B with itself
Often gives off a byproduct (water, acid) but not always
Examples: amides, esters, carbonates, ethers, ureas, urethanes

## Slide 15: Reactions used to make Polymers
acid
amide
amine
acid
alcohol
ester
alcohol
alcohol
ether
+ H2O
+ H2O
+ H2O

## Slide 16: Bulk or Commodity Polymers
Notes: Relatively few polymers responsible for virtually all polymers sold – these are the bulk or commodity polymers

## Slide 19: MOLECULAR WEIGHT
Mw is more sensitive to higher molecular weights
• Molecular weight, Mi: Mass of a mole of chains.
Lower M
higher M
Notes:   Simple for small molecules
  All the same size
  Number of grams/mole
  Polymers – distribution of chain sizes

## Slide 20: Number and Weight averages

## Slide 21: Molecular Weight Calculation
Example: average mass of a class

## Slide 22: Degree of Polymerization, n
n = number of repeat units per chain
ni = 6

## Slide 23: End to End Distance, r Radius of Gyration, Rg
Here:
n=steps
l=length of step
3D Random walk of n steps of length l

## Slide 24: Molecular Structures
• Covalent chain configurations and strength:
Direction of increasing strength
B
ranched
Cross-Linked
Network
Linear
secondary
bonding

## Slide 25: Polymers – Molecular Shape
Conformation – Molecular orientation can be changed by rotation around the bonds
  note: no bond breaking needed

## Slide 26: Polymers – Molecular Shape
Configurations – to change must break bonds
Stereoisomerism
mirror plane

## Slide 27: Tacticity
Tacticity – stereoregularity of chain
isotactic – all R groups on same side of chain
syndiotactic – R groups alternate sides
atactic – R groups random

## Slide 28: Polyisoprene: geometric isomers
Isoprene
Cis-polyisoprene
Doesn’t crystallize
Natural rubber
Trans-polyisoprene
Crystallizes
Gutta-percha

## Slide 29: Copolymers
two or more monomers polymerized together
random – A and B randomly vary in chain
alternating – A and B alternate in polymer chain
block – large blocks of A alternate with large blocks of B
graft – chains of B grafted on to A backbone
  A – B –
random
block
graft
alternating

## Slide 30: Amorphous vs. Semicrystalline Polymers
Amorphous
  Clear
  Soluble
  Usually brittle
  PS, PMMA, PC, unstretched PI
Semicrystalline
  Cloudy
  Not so soluble
  Usually tough
  PE, PP, Nylons, stretched PI

## Slide 31: Polymer Crystallinity
Ex: polyethylene unit cell
Crystals must contain the polymer chains in some way
  Chain folded structure
10 nm

## Slide 32: PE unit cell: 2x2x2 shown
[001]
[010]
[100]
a=0.741 nm
b=0.494 nm
c=0.255 nm
Vuc = a b c

## Slide 34: Polymer Crystallinity
Polymers rarely 100% crystalline
Too difficult to get all those chains aligned
• % Crystallinity: % of material that is crystalline.
-- TS and E often increase
with % crystallinity.
-- Annealing causes
crystalline regions
to grow. % crystallinity
increases.
crystalline
region
amorphous
region

## Slide 35: Degree of crystallinity
Vs = Vc + Va
ms= mc + ma
rsVs = rcVc + raVa
Vc/Vs= (rs-rc)/(rc-ra)=fc
xc = mc/ms = rcVc/ rsVs
xc = (rc/rs)(rs-ra)/(rc-ra)
xc = fc (rc/rs)
Volume fraction
degree of crystallinity
Mass or weight fraction
degree of crystallinity
rc > rs > ra
Typically, crystals more dense:

## Slide 36: Polymer Crystal Forms
Single crystals – only if slow careful growth from dilute solutions

## Slide 37: Polymer Crystal Forms
Spherulite surface
Nucleation site
Spherulites – fast growth from melts – forms lamellar (layered) structures

## Slide 38: Spherulites – crossed polarizers
Maltese cross

## Slide 39: Determining Degree of Crystallinity Xc
Thermal measurements: DSC
  Xc = DH/DH0
X-ray Diffraction
  Xc = Ic/It = Ic/(Ic + Ia)
Density Measurements: Gradient Column
  Xc = [rc(rs-ra)] / [rs(rc-ra)]
  rs density of sample
  ra density of amorphous
  rc density of crystal
  Usually rc > rs > ra