## Slide 2
Each structure has its own atomic packing factor, relationship between atomic radius (r) and unit cell length (a).

## Slide 3
Selenite Crystals in Naica, Mexico
Quartz Crystals – SiO2

## Slide 5: Chemical Composition & Structure (Polymorphism)

## Slide 7: Imperfections in Solids
Solidification- result of casting of molten material
  2 steps
    Nuclei form
    Nuclei grow to form crystals – grain structure
Start with a molten material – all liquid
Crystals grow until they meet each other
nuclei
crystals growing
grain structure
liquid

## Slide 8: Polycrystalline Materials
Grain Boundaries
regions between crystals
transition from lattice of one region to that of the other
slightly disordered
low density in grain boundaries
  high mobility
  high diffusivity
  high chemical reactivity

## Slide 9: Polymer Crystallinity
Ex: polyethylene unit cell
Crystals must contain the polymer chains in some way
  Chain folded structure
10 nm

## Slide 10: Dislocation Motion
Dislocations & plastic deformation
Cubic & hexagonal metals - plastic deformation by plastic shear or slip where one plane of atoms slides over adjacent plane by defect motion (dislocations).
If dislocations don't move, plastic deformation doesn't occur!
Adapted from Fig. 7.1, Callister 7e.
Notes: So we saw that above the yield stress plastic deformation occurs. But how? In a perfect single crystal for this to occur every bond connecting tow planes would have to break at once! Large energy requirement
Now rather than entire plane of bonds needing to be broken at once, only the bonds along dislocation line are broken at once.

## Slide 11: Strengthening Strategies
1. Grain Size
2. Alloying
3. Precipitates
4. Dislocations

## Slide 12: Solid-state Diffusion
• Interdiffusion: In an alloy, atoms tend to migrate
from regions of high conc. to regions of low conc.
Initially
After some time

## Slide 14: Tensile Strength, TS
• Metals: occurs when noticeable necking starts.
• Polymers: occurs when polymer backbone chains are
aligned and slip past one another.
y
strain
Typical response of a metal
F = fracture or
ultimate
strength
Neck – acts as stress concentrator
engineering
TS
stress
engineering strain
• Maximum stress on engineering stress-strain curve.

## Slide 18: Exam I Review
MSEG 302 Spring 2018
Prof. David C. Martin

## Slide 19: Chapter 1: Overview
Introduction to Materials Science and Engineering
Metals, Polymers, Ceramics
Application: Hip Implant
Mechanical Properties vs. Density
Electrical, Magnetic, Optical Properties
Deterioration
Selection: Application -> Properties -> Materials -> Processing

## Slide 20: Chapter 2: Bonding
Atoms: protons, mass, electrons
Wave functions, energy levels
Electronic structure
Periodic table, electronegativity
Ionic bonds, potential energy of interactions
Metallic bonds
Covalent bonds
sp3, sp2 hybridization, chirality
Structure, properties from bond energy curves: r0, Tm, a, E

## Slide 21: Chapter 3: Crystals
Unit cell: a, b, c, a, b, g
SC, BCC, FCC, HCP
Density = mass / volume
Single crystals, polycrystals
Polymorphism
Crystal point coordinates x, y, z; directions [hkl], planes (hkl)
Linear and planar densities
X-ray diffraction

## Slide 22: Chapter 14: Molecules and Polymers
Long-chain molecules
Molecular weights, Mn, Mw
Hydrocarbons, sp2 -> sp3
Chain-growth, step-growth polymerizations
Common reactions, molecular structures
Tacticity
Copolymers
Amorphous vs. Semi-crystalline materials
Degree of Crystallinity

## Slide 23: Chapter 4: Defects
Point Defects: vacancies, interstitials, substitutions
Line Defects: dislocations: edge, screw
Area Defects: grain boundaries, surfaces
Structure, energetics, mobility, influence on properties
Composition by weight/mass, mole/number, volume
Microscopy: optical, electron, scanned probe

## Slide 24: Chapter 5: Diffusion
Diffusion coefficient D = x2/t
Temperature dependence: D= D0 exp(-Qd/RT)
Mechanisms of Diffusion
Fick’s 1st law: J = -D dc/dx (steady-state)
Fick’s 2nd law: dc/dt = D d2c/dx2 (non-steady-state)
Dependence of D on structure, bonding, density, temperature, atom size

## Slide 25: Chapter 6: Mechanics
Engineering stress, strain
Linear, non-linear deformation
Elastic, plastic deformation
Tensile modulus E, Poisson’s ratio v
Shear modulus G, Bulk modulus K
Yield strength (0.2% plastic strain, 0.5% total strain)
Tensile strength
Resilience

## Slide 26: Chapter 6: Mechanics continued
Ductility
Energy to Failure
Hardness testing
True stress, strain
Hardening
Variability: means, standard deviations
Safety factors in design

## Slide 27: Chapter 7: Deformation Mechanisms
Dislocations and slip
Critical resolved shear stress
Grain size
Alloying
Precipitates
Cold working
Annealing: Recovery, Recrystallization, Grain-Growth