## Slide 1: Chapter 5: Diffusion in Solids
ISSUES TO ADDRESS...
• How does diffusion occur?
• Why is it an important part of processing?
• How can the rate of diffusion be predicted for
some simple cases?
• How does diffusion depend on structure
and temperature?

## Slide 2: Diffusion
Diffusion - Mass transport by atomic motion
Mechanisms
Gases & Liquids – random (Brownian) motion
Crystalline Solids – vacancy diffusion or interstitial diffusion
Notes: Diffusion mechanism depends on material

## Slide 3: Processing Using Diffusion
• Case Hardening:
--Diffuse carbon atoms
into the host iron atoms
at the surface
--Example of interstitial
diffusion is a case
hardened gear
• Result: The presence of C atoms makes iron (steel) harder

## Slide 4: Processing Using Diffusion
• Doping silicon with phosphorus for n-type semiconductors:
• Process:
3. Result: Doped
semiconductor
regions.
silicon
2. Heat it.
1. Deposit P rich
layers on surface.
silicon
Color coded atomic maps of element
distribution in a Si device (EDS)

## Slide 5: Solid-state Diffusion
• Interdiffusion: In an alloy, atoms tend to migrate
from regions of high conc. to regions of low conc.
Initially
After some time

## Slide 6: Solid-state Diffusion
• Self-diffusion: In an elemental solid, atoms also migrate
Label some atoms
After some time
A
B
C
D
A
B
C
D

## Slide 7: Diffusion Mechanisms
Vacancy Diffusion:
• atoms exchange with vacancies
• applies to substitutional impurity atoms
• rate depends on:
--number of vacancies
--activation energy to exchange
increasing elapsed time

## Slide 8: Diffusion Simulations
• Simulation of
interdiffusion
across an interface:
• Rate of substitutional
diffusion depends on:
--vacancy concentration
--frequency of jumping.
1. Diffusion couple between A/B
2. Slice with fixed amount of material
3. Source at edge of sample

## Slide 9: Diffusion Mechanisms
Interstitial diffusion – smaller atoms can diffuse between atoms.
More rapid than vacancy diffusion
Notes: this is essentially mechanism in amorphous materials such as polymer membranes

## Slide 10: Diffusion
How do we quantify the amount or rate of diffusion?
Fick’s first law of diffusion
  Flux proportional to concentration gradient =
D  diffusion coefficient

## Slide 11: Steady-State Diffusion
C1
C2
x
C1
C2
x1
x2
Rate of diffusion independent of time

## Slide 12: Diffusion Coefficient
Rates of diffusion determined by D, the diffusion coefficient
D = (distance moved)2 / time = x2/t
  Typical units: cm2/sec or m2/sec
D for gases: ~0.2 cm2/sec
D for liquids: ~2 x 10-5 cm2/sec
D for solids: ~2 x 10-9 cm2/sec
Details depend on chemistry, temperature

## Slide 13: Example: Chemical Protective Clothing (CPC)
Methylene chloride is a common ingredient of paint removers. Besides being an irritant, it also may be absorbed through skin. When using this paint remover, protective gloves should be worn.
If butyl rubber gloves (0.04 cm thick) are used, what is the diffusive flux of methylene chloride through the glove?
Data:
  diffusion coefficient in butyl rubber: D = 110 x10-8 cm2/s
  surface concentrations:
C2 = 0.02 g/cm3
C1 = 0.44 g/cm3

## Slide 14: Example (cont).
glove
C1
C2
skin
paint
remover
x1
x2
Solution – assuming linear conc. gradient
D = 110 x 10-8 cm2/s
C2 = 0.02 g/cm3
C1 = 0.44 g/cm3
x2 – x1 = 0.04 cm
Data:

## Slide 15: Diffusion and Temperature
• Diffusion coefficient increases with increasing T.
D
=
Do
exp
æ
è
ç
ö
ø
-
Qd
R
T
= pre-exponential [m2/s]
= diffusion coefficient [m2/s]
= activation energy [J/mol or eV/atom]
= gas constant [8.314 J/mol-K]
= absolute temperature [K]
D
Do
Qd
R
T

## Slide 16: Diffusion and Temperature
D has exponential dependence on T
D
interstitial
>> D
substitutional
C in a-Fe
C in g-Fe
Al in Al
Fe in a-Fe
Fe in g-Fe
1000 K/T
D (m2/s)
C in a-Fe
C in g-Fe
Al in Al
Fe in a-Fe
Fe in g-Fe
0.5
1.0
1.5
10-20
10-14
10-8
T(C)
1500
1000
600
300
Hot
Cold

## Slide 17
Example: At 300ºC the diffusion coefficient and activation energy for Cu in Si are
D(300ºC) = 7.8 x 10-11 m2/s
Qd = 41.5 kJ/mol
What is the diffusion coefficient at 350ºC?
transform data
D
Temp = T
ln D
1/T

## Slide 18: Example (cont.)
T1 = 273 + 300 = 573 K
T2 = 273 + 350 = 623 K
D2 = 15.7 x 10-11 m2/s

## Slide 19: Other factors
Diffusion FASTER for...
• open crystal structures
• materials w/secondary
bonding
• smaller diffusing atoms
• lower density materials
Diffusion SLOWER for...
• close-packed structures
• materials w/covalent
bonding
• larger diffusing atoms
• higher density materials

## Slide 20: Non-steady State Diffusion
The concentration of diffusing species is a function of both time and position C = C(x,t)
In this case Fick’s Second Law is used
Fick’s Second Law
Note: similar Mathematics also applies for heat transfer
problems: C becomes temperature T, D becomes k
(thermal diffusivity )
Notes: In the non-steady state the concentration profile develops with time.

## Slide 21: Non-steady State Diffusion
Adapted from Fig. 5.5, Callister 7e.
B.C. at t = 0, C = Co for 0  x  
at t > 0, C = CS for x = 0 (const. surf. conc.)
C = Co for x = 
• Copper diffuses into a bar of aluminum.
pre-existing conc., Co of copper atoms
Surface conc.,
C
of Cu atoms
bar
s
C
s

## Slide 22: Solution:
C(x,t) = Conc. at point x at time t
erf (z) = error function
erf(z) values are given in Table 5.1
CS
Co
C(x,t)

## Slide 23: Non-steady State Diffusion
Sample Problem: An FCC iron-carbon alloy initially containing 0.20 wt% C is carburized at an elevated temperature and in an atmosphere that gives a surface carbon concentration constant at 1.0 wt%. If after 49.5 h the concentration of carbon is 0.35 wt% at a position 4.0 mm below the surface, determine the temperature at which the treatment was carried out.
Solution: use Eqn. 5.5

## Slide 24: Solution (cont.):
  t = 49.5 h x = 4 x 10-3 m
  Cx = 0.35 wt% Cs = 1.0 wt%
  Co = 0.20 wt%
 erf(z) = 0.8125

## Slide 25: Solution (cont.):
We must now determine from Table 5.1 the value of z for which the error function is 0.8125. An interpolation is necessary as follows
z
erf(z)
0.90 0.7970
z 0.8125
0.95 0.8209
z = 0.93
Now solve for D

## Slide 26
To solve for the temperature at which D has above value, we use a rearranged form of Equation (5.9a);
from Table 5.2, for diffusion of C in FCC Fe
Do = 2.3 x 10-5 m2/s Qd = 148,000 J/mol

Solution (cont.):
T = 1300 K = 1027°C