## Slide 1: Exam II Review Processing Materials
David C. Martin MSEG 302
The University of Delaware

## Slide 2: Exam II
Chapter 8: Fracture and Failure: HW #7
Chapter 9: Phase Diagrams:
Chapter 10: Phase Transformations, Fe-C alloys: HW#8
Chapter 12: Ceramics
Chapter 15: Polymers: Processing: HW #9
Materials Processing Techniques

## Slide 3: Chapter 8: Fracture and Failure
Stress concentrations at cracks
Critical stress for crack propagation
Fracture toughness
Impact testing
Fatigue testing: S-N curves, da/dN vs. DK
Creep
Steady-state creep:

## Slide 4: Chapter 9: Phase Diagrams
Show stable phases at composition, temperature
Solubility limits, relative amounts, melting, precipitation, transitions
Single phase solutions, two-phase mixtures
Compositions, lever rule for amounts in two-phase regions
Eutectic, eutectoid, peretectic, peritectoid
Composition variations (coring) during cooling
Phase transformations, Fe-C phase diagram near eutectoid

## Slide 5: Chapter 10: Phase Transformations
Fastest rates at optimal amounts of undercooling
Larger structures at higher temperatures, but takes longer
Fe-C (steel):
  Austenite (FCC above eutectoid)
  Coarse Pearlite (ferrite + cementite layers, large)
  Fine Pearlite (ferrite + cementite layers, small)
  Bainite (lath or needle shaped ferrite + cementite)
  Martensite (BCT, diffusionless, hard and brittle)
  Tempered Martensite
  Spheroidite (after extended annealing)
Hypoeutectoid: pro-eutectoid ferrite
Hypereutectoid: pro-eutectoid cementite

## Slide 6: Chapter 12: Ceramics
Anions and cations, strong bonds, brittle and hard
Coordination, relative sizes
Density, structure
Crystals, layers, other structures possible
Defects: need to maintain charge neutrality
Phase diagrams to describe stability, structures

## Slide 7: Polymer properties and processing
Time-temperature dependent properties
Molecular weight, crystallinity, crosslinking
Orientation, drawing
Additives
Processing techniques

## Slide 8: Processing Plastics - Molding
Compression and transfer molding
  thermoplastic or thermoset
Notes: Male & female parts to mold

## Slide 9: Processing Plastics – Extrusion
Notes:   An extruder is a device that used a large screw to melt a polymer, compress it, & force it into a mold
  Extremely commonly used

## Slide 10: Processing Plastics - Molding
Injection molding
  thermoplastic & some thermosets
Notes:   Polymer is melted in chamber & then the molten polymer is forced under pressure into the die

## Slide 11: Polymer Types: Elastomers
Elastomers – rubber
Crosslinked materials
  Natural rubber
  Synthetic rubber and thermoplastic elastomers
    SBR- styrene-butadiene rubber
styrene
– Silicone rubber
butadiene
styrene

## Slide 12: Polymer Types: Fibers
Fibers – have length/diameter >100
Textiles, reinforcements
Formed by spinning
  Extrude polymer through a spinnerette
  May be done from the melt, or from solution

## Slide 13: Fiber spinning
Melt spinning
From the melt, only need to cool
Fastest, requires thermoplastics: PE, PP, PET, Nylons
Wet spinning
  From solution, coagulate in non-solvent
  Rayon (functionalized cellulose)
Dry spinning
  From solution, evaporate solvent
  MPDI (Nomex)
Dry-Jet Wet spinning
From liquid crystal solution
PPTA (Kevlar)
Gel spinning
  From a solidified (crystallized) dilute solution
  UHMWPE (Spectra)

## Slide 14: Polymer Types
Coatings – thin film on surface – i.e. paint, varnish
  To protect item
  Improve appearance
  Electrical insulation
Adhesives – produce bond between two adherands
  Usually bonded by:
    Secondary bonds
    Mechanical bonding
Films – blown film extrusion
Foams – gas bubbles in plastic

## Slide 15: Blown-Film Extrusion

## Slide 16: Conjugated, Conducting Polymers
Sensors
Actuators
Displays
Both electronic
and ionic
conduction

## Slide 17: Summary
• General drawbacks to polymers:
-- E, sy, Kc, Tapplication are generally (but not always) small.
-- Deformation is often T and time dependent.
-- Result: polymers benefit from composite reinforcement.
• Thermoplastics (PE, PS, PP, PC):
-- Smaller E, sy, Tapplication
-- Larger Kc
-- Easier to form and recycle
• Elastomers (rubber):
-- Large reversible strains!
• Thermosets (epoxies, polyesters):
-- Larger E, sy, Tapplication
-- Smaller Kc

## Slide 18: Refinement of Iron from Ore
Iron Ore
Coke
Limestone
3CO +
Fe2O3
®
2Fe
+3CO2
C
+
O2
®
CO2
CO2
+
C
®
2CO
CaCO3
®
CaO+CO2
CaO + SiO2 + Al2O3
®
slag
purification
reduction of iron ore to metal
heat generation
Molten iron
BLAST FURNACE
slag
air
layers of coke
and iron ore
gas
refractory
vessel
Pig Iron: 3.5-4.5%C (near eutectic)

## Slide 19
Bessemer process: reduce carbon content by blowing air on liquid iron
Oxidation reactions release heat, remove carbon
Ladle tipped after conversion to separate from slag (floats)

## Slide 20: Making steel: Basic Oxygen Furnace

## Slide 21: Metal Fabrication
How do we fabricate metals?
  Blacksmith - hammer (forged)
  Molding - cast
Forming Operations
  Rough stock formed to final shape
  Hot working vs. Cold working
  • T high enough for • well below Tm recrystallization work hardening
  • Larger deformations • smaller deformations

## Slide 22: Metal Fabrication Methods - I
FORMING
roll
A
o
A
d
roll
• Rolling (Hot or Cold Rolling)
(I-beams, rails, sheet & plate)
A
o
A
d
force
die
blank
force
• Forging (Hammering; Stamping)
(wrenches, crankshafts)
often at
elev. T
Adapted from Fig. 11.8, Callister 7e.
ram
billet
container
container
force
die holder
die
A
o
A
d
extrusion
• Extrusion
(rods, tubing)
ductile metals, e.g. Cu, Al (hot)
tensile
force
A
o
A
d
die
die
• Drawing
(rods, wire, tubing)
die must be well lubricated & clean
CASTING
JOINING

## Slide 23: Metal Fabrication Methods - II
FORMING
CASTING
JOINING
Casting- mold is filled with metal
  metal melted in furnace, perhaps alloying elements added. Then cast in a mold
  most common, cheapest method
  gives good production of shapes
  weaker products, internal defects
  good option for brittle materials

## Slide 24: Metal Fabrication Methods - II
• Sand Casting
(large parts, e.g.,
auto engine blocks)
trying to hold something that is hot
what will withstand >1600ºC?
cheap - easy to mold => sand!!!
pack sand around form (pattern) of desired shape
Sand
Sand
molten metal
FORMING
CASTING
JOINING

## Slide 25: Metal Fabrication Methods - II
plaster
die formed
around wax
prototype
• Sand Casting
(large parts, e.g.,
auto engine blocks)
• Investment Casting
(low volume, complex shapes
e.g., jewelry, turbine blades)
Investment Casting
pattern is made from paraffin.
mold made by encasing in plaster of paris
melt the wax & the hollow mold is left
pour in metal
wax
FORMING
CASTING
JOINING
Sand
Sand
molten metal

## Slide 26: Metal Fabrication Methods - II
plaster
die formed
around wax
prototype
• Sand Casting
(large parts, e.g.,
auto engine blocks)
• Investment Casting
(low volume, complex shapes
e.g., jewelry, turbine blades)
wax
• Die Casting
(high volume, low T alloys)
• Continuous Casting
(simple slab shapes)
molten
solidified
FORMING
CASTING
JOINING
Sand
Sand
molten metal

## Slide 27
Thixomolding: Magnesium
Lightweight, high precision
electronic components (Mg)
Done from solid + liquid region of the phase diagram
http://www.thixomat.com/

## Slide 28: Metal Fabrication Methods - III
CASTING
JOINING
• Powder Metallurgy
(materials w/low ductility)
pressure
heat
point contact
at low T
densification
by diffusion at
higher T
area
contact
densify
• Welding
(when one large part is
impractical)
• Heat affected zone:
(region in which the
microstructure has been
changed).
piece 1
piece 2
fused base metal
filler metal (melted)
base
metal (melted)
unaffected
unaffected
heat affected zone
FORMING

## Slide 29: Thermal Processing of Metals
Annealing: Heat to Tanneal, then cool slowly.
Types of
Annealing
•
Process Anneal:
Negate effect of
cold working by
(recovery/
recrystallization)
•
Stress Relief: Reduce
stress caused by:
-plastic deformation
-non-uniform cooling
-phase transform.
•
Normalize
(steels):
Deform steel with large
grains, then normalize
to make grains small.
•
Full Anneal
(steels):
Make soft steels for
good forming by heating
to get
g
, then cool in
furnace to get coarse P.
•
Spheroidize
(steels):
Make very soft steels for
good machining. Heat just
below TE & hold for
15-25 h.

## Slide 30: Annealing Temperatures
www.efunda.com

## Slide 31: Ceramic Fabrication Methods-I
• Pressing:
GLASS
FORMING
Gob
Parison
mold
Pressing
operation
• Blowing:
suspended
Parison
Finishing
mold
Compressed
air
plates, dishes, cheap glasses
--mold is steel with graphite lining
• Fiber drawing:
wind up
PARTICULATE FORMING
CEMENTATION

## Slide 32: Sheet Glass Forming
Sheet forming – continuous draw
  originally sheet glass was made by “floating” glass on a pool of mercury

## Slide 33: Heat Treating Glass
• Annealing:
--removes internal stress caused by uneven cooling.
• Tempering:
--puts surface of glass part into compression
--suppresses growth of cracks from surface scratches.
--sequence:
further cooled
tension
compression
compression
before cooling
hot
surface cooling
hot
cooler
cooler
--Result: surface crack growth is suppressed.

## Slide 34: Ceramic Fabrication Methods-IIA
• Milling and screening: desired particle size
• Mixing particles & water: produces a "slip"
• Form a "green" component
• Dry and fire the component
ram
billet
container
container
force
die holder
die
A
o
A
d
extrusion
--Hydroplastic forming:
extrude the slip (e.g., into a pipe)
solid component
--Slip casting:
hollow component
pour slip
into mold
drain
mold
“green
ceramic”
pour slip
into mold
absorb water
into mold
“green
ceramic”
GLASS FORMING
PARTICULATE
FORMING
CEMENTATION

## Slide 35: Clay Composition
A mixture of components used
(50%) 1. Clay
(25%) 2. Filler – e.g. quartz (finely ground)
(25%) 3. Fluxing agent (Feldspar)
binds it together
aluminosilicates + K+, Na+, Ca+

## Slide 36: Features of a Slip
• Clay is inexpensive
• Adding water to clay
-- allows material to shear easily
along weak van der Waals bonds
-- enables extrusion
-- enables slip casting
• Structure of
Kaolinite Clay:
weak van
der Waals
bonding
charge
neutral
charge
neutral
Si
4+
Al
3
+
-
OH
O
2-
Shear
Shear

## Slide 37: Drying and Firing
• Drying: layer size and spacing decrease.
Drying too fast causes sample to warp or crack due to non-uniform shrinkage
wet slip
partially dry
“green” ceramic
• Firing:
--T raised to (900-1400°C)
--vitrification: liquid glass forms from clay and flows between
SiO2 particles. Flux melts at lower T.
Si02 particle
(quartz)
glass formed
around
the particle
micrograph of
porcelain
70 mm

## Slide 38: Ceramic Fabrication Methods-IIB
Sintering: useful for both clay and non-clay compositions.
• Procedure:
-- produce ceramic and/or glass particles by grinding
-- place particles in mold
-- press at elevated T to reduce pore size.
• Aluminum oxide powder:
-- sintered at 1700°C
for 6 minutes.
15 m
GLASS FORMING
PARTICULATE
FORMING
CEMENTATION

## Slide 39: Powder Pressing
Sintering - powder touches - forms neck & gradually neck thickens
  add processing aids to help form neck
  little or no plastic deformation
  Uniaxial compression - compacted in single direction
  Isostatic (hydrostatic) compression - pressure applied by fluid - powder in rubber envelope
  Hot pressing - pressure + heat

## Slide 40: Tape Casting
thin sheets of green ceramic cast as flexible tape
used for integrated circuits and capacitors
cast from liquid slip (ceramic + organic solvent)

## Slide 41: Ceramic Fabrication Methods-III
• Produced in extremely large quantities.
• Portland cement:
-- mix clay and lime bearing materials
-- calcinate limestone (heat to 1400 C: CaCO3 -> CaO + H2O)
-- primary constituents:
tri-calcium silicate (3CaO-SiO2)
di-calcium silicate (2CaO-SiO2)
• Adding water
-- produces a paste which hardens
-- hardening occurs due to hydration (chemical reactions
with the water CaO + H2O -> Ca(OH)2).
• Forming: done usually minutes after hydration begins.
Concrete: cement plus aggregate (gravel)
GLASS FORMING
PARTICULATE
FORMING
CEMENTATION