## Slide 1: Chapter 6: Mechanical Properties
ISSUES TO ADDRESS...
• Stress and strain: What are they and why are
they used instead of load and deformation?
• Elastic behavior: When loads are small, how much
deformation occurs? What materials deform least?
• Plastic behavior: At what point does permanent deformation occur? What materials are most resistant to permanent deformation?
• Toughness and ductility: What are they and how
do we measure them?

## Slide 2: Elastic Deformation
Elastic means reversible!
1. Initial
2. Small load
3. Unload
F
d
bonds
stretch
return to
initial
F
d
Linear-
elastic
Non-Linear-
elastic

## Slide 3: Plastic Deformation (Metals)
Plastic means permanent!
F
d
linear
elastic
linear
elastic
d
plastic
1. Initial
2. Small load
3. Unload
p
lanes
still
sheared
F
d
elastic + plastic
bonds
stretch
& planes
shear
d
plastic

## Slide 4: Common States of Stress
• Simple tension: cable
A
o
= cross sectional
area (when unloaded)
F
F
o
s
=
F
A
o
t
=
F
s
A
s
s
M
M
A
o
2R
F
s
A
c
• Torsion (a form of shear): drive shaft
Ski lift (photo courtesy P.M. Anderson)
In this case stress varies from center to surface of rod

## Slide 5: OTHER COMMON STRESS STATES (1)
(photo courtesy P.M. Anderson)
Canyon Bridge, Los Alamos, NM
o
s
=
F
A
• Simple compression:
Note: compressive
structure member
(s < 0 here).
(photo courtesy P.M. Anderson)
A
o
Balanced Rock, Arches
National Park

## Slide 6: OTHER COMMON STRESS STATES (2)
• Bi-axial tension:
• Hydrostatic compression:
Pressurized tank
s < 0
h
(photo courtesy
P.M. Anderson)
(photo courtesy
P.M. Anderson)
Fish under water
s
z
> 0
s
q
> 0

## Slide 7: Engineering Stress
 Stress has units: N/m2 or lbf/in2
• Shear stress, t:
Area, A
F
t
F
t
F
s
F
F
F
s
t
=
F
s
A
o
• Tensile stress, s:
original area
before loading
Area, A
F
t
F
t
s
=
F
t
A
o
2
f
2
m
N
or
in
lb
=

## Slide 8: Engineering Strain
• Tensile strain:
• Lateral strain:
• Shear strain:
Strain is always
dimensionless.
q
90º
90º - q
y
x
q
g = Dx/y = tan
e
=
d
L
o
-
d
e
L
=
L
w
o
d
/2
d
L
/2
L
o
w
o

## Slide 9: Stress-Strain Testing
• Typical tensile test machine
specimen
extensometer
• Typical tensile specimen
Adapted from Fig. 6.2,
Callister 7e.
gauge
length
Measure F, d; convert to s, e; plot s vs. e

## Slide 10: Linear Elastic Properties
• Modulus of Elasticity, E:
(also known as Young's modulus)
• Hooke's Law:
s = E e
s
Linear-
elastic
E
e
F
F
simple
tension
test

## Slide 11: Poisson's ratio, n
• Poisson's ratio, n:
Units:
E: [GPa] or [psi]
n: dimensionless
   > 0.50 density increases
   < 0.50 density decreases (voids form)
eL
e
-
n
e
n
=
-
L
e
metals: n ~ 0.33 ceramics: n ~ 0.25 polymers: n ~ 0.40

## Slide 12: Energies and Forces

## Slide 13: Mechanical Properties
Slope of stress strain plot (which is proportional to the elastic modulus) depends on bond strength
Adapted from Fig. 6.7,
Callister 7e.

## Slide 14: Other Elastic Properties
• Elastic Shear
modulus, G:
t
G
g
t = G g
simple
torsion
test
M
M
• Special relations for isotropic materials:
2(1 + n)
E
G
=
3(1 - 2n)
E
K
=
• Elastic Bulk
modulus, K:
pressure
test: Init.
vol =Vo.
Vol chg.
= DV
P
P
P
P = -
K
D
V
V
o
P
D
V
K
V
o

## Slide 15: Young’s Moduli: Comparison
Metals
Alloys
Graphite
Ceramics
Semicond
Polymers
Composites
/fibers
E(GPa)
Based on data in Table B2,
Callister 7e.
Composite data based on
reinforced epoxy with 60 vol%
of aligned
carbon (CFRE),
aramid (AFRE), or
glass (GFRE)
fibers.
109 Pa
0.2
8
0.6
1
Magnesium,
Aluminum
Platinum
Silver, Gold
Tantalum
Zinc, Ti
Steel, Ni
Molybdenum
G
raphite
Si crystal
Glass
-
soda
Concrete
Si nitride
Al oxide
PC
Wood( grain)
AFRE( fibers)
*
CFRE
*
GFRE*
Glass fibers only
Carbon
fibers only
A
ramid fibers only
Epoxy only
0.4
0.8
2
4
6
10
2
0
4
0
6
0
8
0
10
0
2
00
6
00
8
00
10
00
1200
4
00
Tin
Cu alloys
Tungsten
<100>
<111>
Si carbide
Diamond
PTF
E
HDP
E
LDPE
PP
Polyester
PS
PET
C
FRE( fibers)
*
G
FRE( fibers)*
G
FRE(|| fibers)*
A
FRE(|| fibers)*
C
FRE(|| fibers)*

## Slide 16: Plastic (Permanent) Deformation
(at lower temperatures, i.e. T < Tmelt/3)
• Simple tension test:
engineering stress, s
engineering strain, e
Elastic+Plastic
at larger stress
permanent (plastic)
after load is removed
ep
plastic strain
Elastic
initially

## Slide 17: Yield Strength, sy
• Stress at which noticeable plastic deformation has
occurred.
when ep = 0.002
y = yield strength
Note: for 2 inch sample
 = 0.002 = z/z
 z = 0.004 in
Adapted from Fig. 6.10 (a),
Callister 7e.
tensile stress,
s
engineering strain,
e
sy
e
p
= 0.002

## Slide 18: Alternative Definition of Yield Strength, sy
• Stress at which et=0.005 total strain occurs
y = yield strength
tensile stress,
s
engineering strain
e
sy
e
t
= 0.005
Particularly useful for materials
with no well-defined initial
linear regime (some plastics)

## Slide 19: Yield Strength : Comparison
Room T values
Based on data in Table B4,
Callister 7e.
a = annealed
hr = hot rolled
ag = aged
cd = cold drawn
cw = cold worked
qt = quenched & tempered
Graphite/
Ceramics/
Semicond
Metals/
Alloys
Composites/
fibers
Polymers
Yield strength,
s
y
(MPa)
PVC
Hard to measure
,
since in tension, fracture usually occurs before yield.
Nylon 6,6
LDPE
70
20
40
60
50
100
10
30
2
00
3
00
4
00
5
00
6
00
7
00
10
00
2
0
00
Tin (pure)
Al
(6061)
a
Al
(6061)
ag
Cu
(71500)
hr
Ta
(pure)
Ti
(pure)
a
Steel
(1020)
hr
Steel
(1020)
cd
Steel
(4140)
a
Steel
(4140)
qt
Ti
(5Al-2.5Sn)
a
W
(pure)
Mo (pure)
Cu
(71500)
cw
Hard to measure,
in ceramic matrix and epoxy matrix composites, since
in tension, fracture usually occurs before yield.
H
DPE
PP
humid
dry
PC
PET
¨
Typically
sy ~ E/100

## Slide 20: Tensile Strength, TS
• Metals: occurs when noticeable necking starts.
• Polymers: occurs when polymer backbone chains are
aligned and slip past one another.
y
strain
Typical response of a metal
F = fracture or
ultimate
strength
Neck – acts as stress concentrator
engineering
TS
stress
engineering strain
• Maximum stress on engineering stress-strain curve.

## Slide 21: Tensile Strength : Comparison
Si crystal
<100>
Graphite/
Ceramics/
Semicond
Metals/
Alloys
Composites/
fibers
Polymers
Tensile
strength, TS
(MPa)
PVC
Nylon 6,6
10
100
200
300
1000
Al
(6061)
a
Al
(6061)
ag
Cu
(71500)
hr
Ta
(pure)
Ti
(pure)
a
Steel
(1020)
Steel
(4140)
a
Steel
(4140)
qt
Ti
(5Al-2.5Sn)
a
W
(pure)
Cu
(71500)
cw
L
DPE
PP
PC
PET
20
30
40
2000
3000
5000
Graphite
Al oxide
Concrete
Diamond
Glass-soda
Si nitride
H
DPE
wood
( fiber)
wood(|| fiber)
1
GFRE
(|| fiber)
GFRE
( fiber)
C
FRE
(|| fiber)
C
FRE
( fiber)
A
FRE
(|| fiber)
A
FRE( fiber)
E-glass fib
C
fibers
Aramid
fib
Room Temp. values
Based on data in Table B4,
Callister 7e.
a = annealed
hr = hot rolled
ag = aged
cd = cold drawn
cw = cold worked
qt = quenched & tempered
AFRE, GFRE, & CFRE =
aramid, glass, & carbon
fiber-reinforced epoxy
composites, with 60 vol%
fibers.

## Slide 22: Ductility
• Plastic tensile strain at failure:
Adapted from Fig. 6.13, Callister 7e.
• Another ductility measure:
100
x
A
A
A
RA
%
o
f
o
-
=
x 100
L
L
L
EL
%
o
o
f
-
=
Engineering tensile strain,
e
E
ngineering
tensile
stress,
s
smaller %EL
larger %EL
Lf
Ao
Af
Lo

## Slide 23: Toughness
• Energy to break a unit volume of material
• Approximate by the area under the stress-strain
curve.
Brittle fracture: elastic energy Ductile fracture: elastic + plastic energy
very small toughness
(unreinforced polymers)
Engineering tensile strain,
e
E
ngineering
tensile
stress,
s
small toughness (ceramics)
large toughness (metals)

## Slide 24: Resilience, Ur
Ability of a material to store energy
  Energy stored best in elastic region
If we assume a linear stress-strain curve this simplifies to
Adapted from Fig. 6.15, Callister 7e.
y
y
r
2
1
U
e
s
@

## Slide 25: Elastic Strain Recovery

## Slide 26: Hardness
• Resistance to permanently indenting the surface.
• Large hardness means:
--resistance to plastic deformation or cracking in
compression.
--better wear properties.
e.g.,
10 mm sphere
apply known force
measure size
of indent after
removing load
d
D
Smaller indents
mean larger
hardness.
increasing hardness
most
plastics
brasses
Al alloys
easy to machine
steels
file hard
cutting
tools
nitrided
steels
diamond

## Slide 27: Hardness: Measurement
Rockwell
  No major sample damage
  Each scale runs to 130 but only useful in range 20-100.
  Minor load 10 kg
  Major load 60 (A), 100 (B) & 150 (C) kg
    A = diamond, B = 1/16 in. ball, C = diamond
HB = Brinell Hardness
  TS (psi) = 500 x HB
  TS (MPa) = 3.45 x HB

## Slide 28: Hardness: Measurement
Table 6.5

## Slide 29: True Stress & Strain
Note: S.A. changes when sample stretched
True stress
True Strain
Adapted from Fig. 6.16, Callister 7e.

## Slide 30: Hardening
• Curve fit to the stress-strain response:
s
T
=
K
e
T
(
)
n
“true” stress (F/A)
“true” strain: ln(L/Lo)
hardening exponent:
n =
0.15 (some steels)
to n =
0.5 (some coppers)
• An increase in sy due to plastic deformation.
s
e
large hardening
small hardening
s
y
0
s
y
1

## Slide 31: Variability in Material Properties
Elastic modulus is material property
Critical properties depend largely on sample flaws (defects, etc.); large sample to sample variability
Statistics
  Mean
  Standard Deviation
where here n is the number of data points
Notes: All samples have same value
Because of large variability must have safety margin in engineering specifications

## Slide 32: Design or Safety Factors
• Design uncertainties mean we do not push the limit
• Factor of safety, N
• Example: Calculate a diameter, d, to ensure that yield does
not occur in the 1045 carbon steel rod below. Use a
factor of safety of 5.
5
1045 plain
carbon steel:
s
y
= 310 MPa
TS = 565 MPa
F = 220,000N
d
L
o
d = 0.067 m = 6.7 cm

## Slide 33: Summary
• Stress and strain: These are size-independent
measures of load and displacement, respectively
• Elastic behavior: This reversible behavior often
shows a linear relation between stress and strain
To minimize deformation, select a material with a
large elastic modulus (E or G)
• Toughness: The energy needed to break a unit
volume of material
• Ductility: The plastic strain at failure
• Plastic behavior: This permanent deformation
behavior occurs when the tensile (or compressive)
uniaxial stress reaches sy